## Slide 1: High-pressure phase of calcium: Prediction of phase Ⅵ and upper-pressure phases from first principle
Takahiro Ishikawa,Hitose Nagara,
Naoshi Suzuki,Taku Tsuchiya,
and Jun Tsuchiya
Shimizu lab. ORII Daisuke
Phys.Rev.B 81,092104(2010)

## Slide 2: Contents
Introduction
What’s “High-pressure phase”?
⇒An interesting property
What’s “phase Ⅵ”?
First principles calculations
Motivation
Research
Summary
High-pressure phase of calcium: Prediction of phase Ⅵ and upper-pressure phases from first principle

## Slide 3: What’s “High-pressure phase”?
simple cubic
Pressure
The structure change!!
=Structural phase transition
(構造相転移)
Decreasing inter atomic distance by compression
Electronic states change!
bcc
fcc

## Slide 4: An interesting property pressure-induced superconductivity
Superconductivity(超伝導)
⇒electrical resistance = 0
⇒Meissner effect B=0
linear motor car
electrical cable
@ extremely-low-temperature
Normalconductivity (常伝導)
Superconductivity (超伝導) !!
Phase transition!!
cool

## Slide 5: What’s “phase Ⅵ”?
Matsuoka private communication
①【Ca-Ⅳ structure】
Tetragonal P41212 structure with fourfold helical atomic arrangements
②【Ca-Ⅴ structure】
Orthorhombic Cmca structure with zigzag atomic arrangement
Structural phase transitions (構造相転移) of calcium
fcc
bcc
sc (simple cubic)
①
[GPa]
20
32
113
139
Ca-I
Ca-II
Ca-III
Ca-IV
Ca-V
②
?
⇒ Highest Tc in simple element!
Transition temperature Tc 25K @ 161GPa (Ca-Ⅴ?)
Ca

## Slide 6: First principles calculations
Input data
Crystal structure
Type of atoms
Determination of electronic states
Output data
Charge density
Total energy
Stress
Inter atomic force
etc…

## Slide 7: Motivation
Background
Investigating mechanism of high Tc superconductivity
Predicting the structure of Ca in which the highest Tc is observed
Notes: ・超伝導のメカニズムを調べたいということを大きな背景にして、カルシウムの

## Slide 8: Computational details
structure
fcc
bcc
sc (simple cubic)
hcp
Cmca
Cmcm
Pnma
I41/amd
P41212
I4/mcm(0,0,γ)
The most stable structure @ 0K
Input data
Making crystal structure (lattice vectors and atomic coordinates)
Type of atoms
⇒structural optimization
⇒electronic states
Comparing the enthalpies up to 200Gpa
(enthalpy)
Notes: 過去の研究で著者以外の様々な研究グループによって、カルシウムの高圧相はこれだけ提唱されている。
それぞれ各圧力で最も安定な構造を【構造最適化という手法を用いて決定し、構造間の各圧力でのエネルギー的安定性を調べました。
そのためにエンタルピーという物理量を比較して、安定性についての議論をしました。
「質疑応答」
実験⇒３００Kだが０Kの近似でもうまくいく・・・
有限温度で計算することはできないが、その方法はいろんな研究者によって、考えられている。精度を上げる近似法。
第一原理(英語はfirst-principlesまたはab initio(英語ではない))とは、なんら実験データや経験パラメーターを使わないで理論計算をする方法の総称。でも、この業界では電子状態計算、平たく言うとシュレディンガー方程式を解く計算のことを暗に指すことが多い。したがって、このページも電子状態計算のお話となる。
QUANTUM ESPRESSO code
①Exchange-correlation energy functional
⇒GGA (generalized gradient approximation)
Ten electrons in the 3s,3p,and 4s states
⇒USPP(ultrasoft pseudopotential)
The energy cutoff EC of the plane-wave basis
⇒40Ry
②
The number of the calcium atoms in the unit cell Na
The number of the k-point sampling in the Brillouin zone Nk
fcc (Na=1,Nk=16×16×16)
bcc (Na=1,Nk=16×16×16)
sc (simple cubic) (Na=1,Nk=16×16×16)
hcp (Na=2,Nk=16×16×16)
Cmca (Na=4,Nk=8×8×8)
Cmcm (Na=4,Nk=8×8×8)
Pnma (Na=4,Nk=8×8×8)
I41/am (Na=4,Nk=8×8×8)
P41212 (Na=8,Nk=8×8×8)
I4/mcm(00γ) (Na=32,Nk=4×4×4)

## Slide 9: Comparing enthalpies
figure 1
figure 2
(enthalpy)
The lowest ΔH point
⇒Most stable structure
Notes: 順番に

## Slide 10
Pnma
I4/mcm(00γ)
fcc
bcc
I41/amd
P41212
[GPa]
3.5
32
109
135
Cmca
Pnma
74
117
Ca-I
Ca-II
Ca-IV
Ca-V
Ca-Ⅲ
Ca-VI?
Ca-VII?
I4/mcm(00γ)
[GPa]
495
Ca-VII?
hcp
Ca-VIII?
I4/mcm(00γ)
fcc
bcc
sc (simple cubic)
P41212
[GPa]
20
32
113
139
Ca-I
Ca-II
Ca-III
Ca-IV
Ca-V
Experiment
Calculation in this paper
Cmca
Notes: 最後に余談：Scが第一原理計算で出てこないというのがこの計算の問題点であり、これを解決するために世界中の多くのグループで研究されている。
The sc structure is energetically and mechanically unstable.
Why?
Anharmonicity ?
Thermal effect ?
Beyond LDA (GGA) ?

## Slide 11: Superconductivity
Theoretically ,Tc=25K was obtained around the phase boundary between Ca-Ⅵ and Ca-Ⅶ.
50
100
150
pressure(GPa)
J.Phys. Soc. Jpn. 75, 083703 (2006).
Chart: Prediction
| 100 | 110 | 120
theory | 22 | 19 | 21
線形用 | 19 | 21
109 | 0 | 30
tate2 | 0 | 30
tate3 | 0 | 30
74 | 0 | 30
32 | 0 | 30
3.5 | 0 | 30
Ca-Ⅵ
158(GPa)
Experimental result
(⇒Recently , the structure of Ca-Ⅵ was experimentally confirmed.)
(Y.Nakamoto et al , Phys.Rev.B , 81, 140106(R) (2010).)
Notes: 圧力上昇に伴った構造相転移の様子 : Prediction
Ⅳ、Ⅴ、Ⅵ相各相で、超伝導転移温度を計算→Allen-dynes formula
実験値との比較（Ⅵ相が最近の論文で見つかっている。）順番に。Ⅵ相あたりで25Kを観測。
計算結果から高いTcが観測されるのは、Ⅵ、Ⅶ相あたりだと予測できる。
λ・・・ESPLESSO
μ*・・・0.1
<ω>・・・phonon frecency𝑇_𝑐=(<𝜔>)/1.20 exp⁡{−(1.04(1+𝜆))/(𝜆−𝜇^∗ (1+0.62𝜆))}
Allen-Dynes formula

## Slide 12: Summary
The structures of the phases Ca-Ⅵ and Ca-Ⅶ were predicted.
The highest TC of 25K in
the Ca-Ⅵ or Ca-Ⅶ phase.