## Slide 1
Fe
As
A = Ca, Sr, Ba
Superconductivity in system AFe2(As1-xPx)2
Dulguun Tsendsuren
Kitaoka Lab.
Division of Frontier Materials Sc.
Department of Materials Engineering Sc. Graduate School of Engineering Sc., Osaka Univ.
Evolution from non-Fermi- to Fermi-liquid transport via isovalent doping in BaFe2(As1−xPx)2 superconductors
Kasahara et. al., Phys. Rev. 81, 184519(2010)

## Slide 2: History of Superconductivity
under high pressure
0
50
100
150
200
SmO
0.9
F
0.11
FeAs
LaO
0.89
F
0.11
FeAs
LaOFeP
Hg-Ba-Ca-Cu-O
（
）
Hg-Ba-Ca-Cu-O
Tl-Ba-Ca-Cu-O
Bi-Sr-Ca-Cu-O
Y-Ba-Cu-O
MgB2
Nb
Ge
NbN
NbC
Nb
Pb
high-Tc cuprate
metal
iron-based system
Transition temperature (K)
1900
1920
1940
1960
1980
2000
2020
Year
Hg
La-Ba-Cu-O
Discovery of superconductivity
1911
1986
High-Tc cuprate superconductor
2006
Iron-based high-Tc superconductor
77
163
1979
Heavy fermion superconductor
CeCu2Si2
heavy fermion system
PuCoGa5
Introduction

## Slide 3: Iron-based Superconductors
Introduction
11
111
1111
42226
Today’s talk
Each system has FeAs layer
122
Fe
As

## Slide 4
Introduction
AFe2As2 System
CaFe2As2
SrFe2As2
BaFe2As2
iso-valent doping
Role of FeAs layer in 122 system
CaFe2(As1-xPx)2
SrFe2(As1-yPy)2
BaFe2(As1-zPz)2

## Slide 5
Introduction
Superconducting gap
Structure | Substance | Tc [K]
42622 | CaAlOFeAs | 27
1111 | NdFeAsO | 55
122 | Ba1-xKxFe2As2 | 38
Structure | Substance | Tc [K]
42622 | SrScOFeP | 17
1111 | LaFePO | 5
122 | BaFe2(As1-xPx)2 | 31
Energy
EFermi
Full gap
Density of State
gap
Density of State
Energy
EFermi
Nodal gap
gap
Spin-Lattice Relaxation Rate (by NMR)
Magnetic Penetration Depth
Thermal Conductivity
Specific Heat
Structure | Substance | Tc [K]
42622 | CaAlOFeAs | 27
1111 | NdFeAsO | 55
122 | Ba1-xKxFe2As2 | 38
Structure | Substance | Tc [K]
42622 | SrScOFeP | 17
1111 | LaFePO | 5
122 | BaFe2(As1-xPx)2 | 31
Spin-Lattice Relaxation Rate (by NMR)
Magnetic Penetration Depth
Thermal Conductivity
Specific Heat

## Slide 6
electronic
spin
Releases the energy
T1: spin-lattice relaxation time
nuclear
spin
Spin-Lattice interaction
Energy Transfers in
almost T1 time
I
e
Introduction
Relaxation rate 1/T1 by NMR

## Slide 7
Introduction
How to verify SC gap?
Spin-Lattice Relaxation Rate
(by NMR)
Spin-Lattice relaxation time
Full gap:
Temperature
Non-Linear
relation
Nodal gap:
Temperature
Linear
relation

## Slide 8: Resistivity of BaFe2(As1-xPx)2
Exp. Result
Resistivity:
T0 Structure transition
TSDW AFM Order
Tcon Superconductivity appears
Resistivity reflects phase transition clearly as other transport properties

## Slide 9
Transitions:
Structure
SDW
onset Tc
Bulk Tc
Exp. Result
Phase Diagram of BaFe2(As1-xPx)2
Doping level (x) of P in BaFe2(As1-xPx)2
At x = 0.26
Tcmax = 31 [K]

## Slide 10
Highest Tc is clearly related
to AFM fluctuation
Exp. Result
Resistivity of BaFe2(As1-xPx)2
Resistivity:
Fermi-liquid:
Tc = 0[K]
AFM fluctuation:
(Non-Fermi-liquid)
Tc = 31[K]

## Slide 11
Calculation
Fermi Surfaces vs. Doping
BaFe2As2
BaFe2P2
iso-valent
doping
(P at As)
Ba0.8K0.2Fe2A2
hole doping
(K at Ba)
Nodal gap
Full gap
Full gap shows higher Tc compared with Nodal gap
With 3D like FSs, SC gap becomes Nodal gap
Tcmax = 38[K]
2D like FS
Tcmax = 31[K]
3D like FS

## Slide 12
Tcmax = 15 [K], at x = 0.05
SC occurs in tetragonal structure
In c-Tetra., FS changed into 3D
SC disappears in c-Tetra
Exp. Result
CaFe2(As1-xPx)2
Fermi surfaces:
Tetragonal (SC)
c-Tetra. (NC)

## Slide 13
Summary
Superconductivity occurs:
  AFM fluctuation appears nearby high Tc SC region
  With structural change (Orthorhombic to Tetragonal)
Fermi Surface is structure dependent. In most cases, SC occurs when FSs are like 2D
Essence of Full gap is one of promising key to increase Tc in Superconductivity

## Slide 14
Thank you
for your attention