## Slide 1: Terahertz spectroscopy of electromagnons excitation in a hexaferrite Ba2Mg2Fe12O22
Ashida Lab.
Tadataka Saito
Phy.Rev.B 83, 064422(2011)
Phy.Rev. B 80, 220406(R) (2009)

## Slide 2: Contents
Introduction
Polarization and magnetization
Multiferroics
Electromagnon
Method
THzTDS
Results
Conclusion

## Slide 3: Polarization and Magnetization
+
+
+
+
-
+
+
+
+
-
P
-
-
Polarization
Magnetization
E
H
M
Ferroelectric and Ferromagnetic
M=0
Application for memory devices
Introduction
分極
強誘電性と強磁性
磁化

## Slide 4: Multiferroics
E
H
P
M
Multiferroics are materials where ferroelectricity and
ferromagnetism are inherently coupled.
The magnetization can be controlled by electric field of light.
The polarization can be controlled by magnetic field.
Introduction

## Slide 5: Magnetoelectric effect (ME effect)
In 2003,RMnO3(R; rare earth element)
Polar lattice distortion
Induce Polarization
Ptotal //c
Spiral-spin-order
a
b
c
Antisymmetry
Dzyaloshinskii-Moriya interaction
Introduction
空間格子の反転対称性の歪み
らせんスピン磁性
bc-spiral

## Slide 6: Electromagnon
Magnon can be excited by electric field of light.
Magnon
Introduction
Spin wave
Magnon is exited by magnetic field of light.
Multiferroics
Electromagnon
(2006)

## Slide 7: Theory of electromagnon
Introduction
Ptotal //c
a
b
c
Eω//a
E
Mn
Mn
O
Symmetric exchange interaction
ME effect

## Slide 8: Hexagonal ferrite Ba2Mg2Fe12O22
Ferri magnetic
proper screw
Conical spin
Room temperature
T<195K
T<50K
Introduction
六方晶フェライト
By neutron diffraction

## Slide 9: Transition of spin phase by magnetic field
H//[001]
Longitudinal conical spin
H(>3T)
H//[100]
Transverse conical spin
H(＞4T)
Introduction
Ferrimagnetic
Proper screw
Ferrimagnetic
θ
(001)
(100)
(120)

## Slide 10
THz-TDS enables us to observe a waveform of ”E(t)” directly.
By using THz-TDS , both amplitude and phase of ”E(t)” are directly obtained.
Pump beam
Delay stage
Probe beam
THz-TDS
fs pulse laser
THz emitter
THz detector
sample
Terahertz time-domain spectroscopy (THz-TDS)
Method

## Slide 11: Longitudinal conical form
Results
Conical
Proper-screw
Ferri
Conical
Ferri
Proper
F
C
F
C
F

## Slide 12: Transverse conical form
Results
Conical
Proper
Ferri
Proper-screw
Conical
Ferri
F
C
C
F
F

## Slide 13: Conclusion
・The electromagnon appears only in the conical spin
ordered phase but irrespective of the longitudinal or
the transverse conical form.No electromagnon is
observed in the properscrew or ferrimagnetic phase.
・The symmetric exchange interaction (Si・Sj) is dominant
source of the observed electromagnon.
at room temperature
Electromagnon
Conclusion
Noncolinear spin structure
at room temperature

## Slide 16: Purpose
・To investigate the situation where electromagnon induced
by changing temperature and external magnetic field
・How the intensity of the absorption by electromagnon
depend on the external magnetic field?
Is it possible to induce electromagnon at room temperature?

## Slide 17: Decide optical coefficient
d
Sample
Fourier transformed spectrum
Transmission Fresnel constants

## Slide 18: Experimental set up

## Slide 19: Emergency of electromagnon
depend on the direction of electric field
at conical spin phase(4.3K)
depend on the external magnetic field
(H//[001],4.3K)
Phy.Rev. B 80, 220406(R) (2009)
Absorption by electromagnon is obserbed around 2.8meV(0.7THz).
Results

## Slide 20: Y-type

## Slide 21: Spiral spin structure
反時計回り
時計回り
反転対称性が崩れる
格子歪みによる分極発生

## Slide 22: Electromagnon
………..
H
Magnon
Energy
at THz region
(0.1THz-10THz)
0.41meV-41meV
・observed at THz region
・depends on the direction of electric field
・The intensity of absorption depend on
the external magnetic field.
[001]
[100]
[120]
L
S

## Slide 23: RMnO3 electromagnon