## Slide 1: Fabrication of (Fe,Mn)3O4 nanowires using a sidewall deposition method
Tanaka lab
Takayoshi Kushizaki
M1 colloquium 8/6/2011
(サイドウォール蒸着を用いた(Fe,Mn)3O4ナノワイヤーの作製)

## Slide 2
Contents
・background of my research
・the method to fabricate nano wires
・structural analysis of nano wires
・summary
My experiment

## Slide 3
Science 285, 1540 (1999)
Ferromagnetic metal
Paramagnetic insulator
(La,Ca)MnO3 thin film
The strongly correlated electron materials oxide
Nano scaled domain structure
VO2 thin film
Science 318, 1750 (2007)
insulator
metal
Giant physical properties in nano structures
(強相関電子系酸化物)
The effect of nano structures

## Slide 4
(La,Pr,Ca)MnO3
J.Appl.Phys. 100, 124316 (2006)
Drastic change by fabricating nano structure
Pick up the intrinsic physical property

## Slide 5
Spinel structure
(Fe3-xMnx)O4 : Mn doped Fe3O4
Appl. Phys. Lett. 86, 222504 (2005)
My target : (Fe3-xMnx)O4
・High spin polaryzation (スピン偏極率)
・high curie temperature(Tc)
・control carrier density by doping Mn
Application for devise
Large MR
Magnetoresistance(MR):
the phenomenon that resistance changes by applied magnetic field

## Slide 6
The method to fabricate nano wires
Sidewall deposition
1.Fabricate wall
2.Deposite target
along with the wall
(蒸着する)
3.Remove the wall
It is possible to fabricate nano wires that height and width are 10-100nm easily.
Control height
Control width
Nano wire

## Slide 7
Fabricate wall using nanoimprint
etching
CF4 plasma
O2 plasma
Nanoimprint
fabrication pattern(wall)
UV
mold
resist2
Al2O3
resist1
resist1:stiffening by heat
resist2:stiffening by UV
10μm

## Slide 8
Deposite target and remove the wall
Target(FMO)
Pulsed laser
Pulsed laser deposition
annealing
FMO nano wire
Ar plasma
solution
immersion(浸漬)
milling
deposition of FMO
1μm
FMO

## Slide 9
250nm
35nm
Structure of FMO nano wires(SEM)
width：30-100nm
height：100-150nm
length：100μm-
100nm
140nm
Cross sectional view
40nm
50μm
Many wires in large field
Top view

## Slide 10
Transmission Electron Microscope(TEM)
(透過型電子顕微鏡)
TEM
・high resolution (0.1nm-)
・diffraction image
→identification of material,
analysis of crystal condition
TEM image
（Ta2O5）MOS structure
polycrystal
Selected area diffraction image
monocrystal

## Slide 11
50nm
Al2O3
Al
resin(樹脂)
Al2O3
wires＋Al2O3
FMOナノワイヤーの構造解析
I succeeded in fabrication of polycrystal nano wires.
Structural analysis of FMO nanowire(TEM)
TED Image
(321)FMO
(310)FMO
(111)FMO
(210)FMO
FMO
[0001]Al2O3
[1100]Al2O3
[1120] Al2O3

## Slide 12
Summary
・I established the process that fabricates FMO nano wires using a sidewall deposition method.
・I succeeded in fabrication of polycrystal FMO nano wires which were width 30-100nm,height 50-150nm, length100μm over.
I will investigate the MR property of a nano wire.

## Slide 13
Magnetoresistance(MR)
(磁気抵抗効果)
Magnetoresistance(MR):
the phenomenon that resistance changes by applied magnetic field
Application devise
(磁気メモリ)
・nonvolatile
・fast reading and writing speed
The ultimate memory
insulator
ferromagnetics
H
MRAM
current
TMR junction

## Slide 14
MR (thin film vs wires)
Nano wires have a MR property that is similar to poly and epi films.