## Slide 1: Switching of Magnetic Ordering in CeRhIn5 under Hydrostatic Pressure
Kitaoka Laboratory
Kazuhiro Nishimoto
N. Aso et al., Phys. Rev. B 78, 073703 (2009).

## Slide 2: Contents
Introduction
- Heavy fermion system
- Motivation
- Crystal and magnetic structure of CeRhIn5
Measurement
- Neutron diffraction
Result
Summary

## Slide 3
Example of heavy fermion superconductor compounds
Example of Heavy Fermion System
UPt3 UPd2Al3
CeCu2Si2 CePd2Si2 CeRh2Si2 CeIn3 CeRhIn5
PrOs4Sb12
PuCoGa5 etc
Introduction

## Slide 4: Property of f electron
Normal metal
Ce3+:･･･5s25p6 4f 1
Heavy Fermion system
n(r)
r
4f
5p
5d
6s
closed shell
Conduction electron
4f
4f
4f
4f
4f
4f
＋
＋
＋
＋
＋
＋
c-f hybridization
＋
＋
＋
＋
＋
＋
Introduction

## Slide 5
Specific heat : C =gT [g = (2/3)p2kB2D(eF)]
Susceptibility : c = c0 [c0 = 2mB 2D(eF)]
Resistivity : r = r0 + AT n [A ∝ ∝g2]
γheavy /γnormal ＝ 100 ~ 1000
“Heavy” ⇒ The effective mass is large
D(εF) is the electronic density of states at the Fermi energy εF .
∝ m* (effective mass)
2
2
)
(
h
2
=
p
e
m*kF
F
D
What does “Heavy” mean？
Introduction

## Slide 6: Two types of interactions
(RKKY:Rudermann-Kittel-Kasuya-Yoshida)
Magnetic Order
Fermi Liquid
4f electron (Ce)
RKKY interaction
The interplay between two 4f electrons mediated by conduction electrons
4f electron (Ce)
Kondo effect
4f and conduction electrons form a spin-singlet state.
heavy fermion system : 重い電子系
Jcf
Jcf
Conduction electron
Jcf
Conduction electron
Polarization
Introduction

## Slide 7: Phase Diagram of HF system
As Jcf increases , AFM disappears
and SC appears (near QCP)
TK ∝ W exp(-1/J cf D(εF))
TRKKY ∝ D(εF) Jcf2
AFM : antiferromagnetism(反強磁性)
HF : heavy fermion(重い電子状態)
QCP : quantum critical point(量子臨界点)
Introduction

## Slide 8: Motivation
SC
AFM
Introduction
CeRhIn5 has a phase that AFM coexists with SC.
Is the AFM order affected by SC?
What happens to magnetic order?
T-P phase diagram for CeRhIn5

## Slide 9
Crystal and magnetic structure of CeRhIn5
P=0 GPa
Propagation wave vector
Q = (0.5, 0.5, ±δ)
Incommensurability : δ
P = 0 GPa: δ = 0.297
Introduction
Neutron diffraction

## Slide 10: Neutron diffraction
Measurement
Neutron diffraction can
reveal magnetic structure.
s = 1/2
X-ray
Brugg reflection
neutron

## Slide 11: Neutron diffraction along the (0.5, 0.5, L) direction in the non-SC state
Results
P ～0.25 GPa
T = 0.73 K
P ～0.93 GPa
T = 0.75 K
P ～1.48 GPa
T = 2.0 K
4.9K
How does δ changes in SC state?
●
●
●
δ increases with increasing P
in the non-SC state.
(a)
(b)
(c)
(a)
(b)
(c)

## Slide 12: Neutron diffraction profiles under P～1.48 GPa
Results
The peak at Q1 gradually lowers
and completely disappears at 0.75 K.
A new peak (Q2) emerges at 0.9 K
and becomes large at 0.75 K.
●
●
●

## Slide 13: T-dependence of the peak intensities
Results
Switching of the two magnetic vectors occurs at Tc.
T(K)
It suggests that the AFM order is affected by the SC.
Pressure evolution of δ

## Slide 14: Summary
In CeRhIn5 , the AFM coexists with the SC under high pressure and low temperature.
Switching of two magnetic ordering vectors (Q1 & Q2) occurs at Tc.
Switching suggests the possibility that the AFM order is affected by the SC.