## Slide 1
Tanaka Lab. Yasushi Fujiwara
Three dimensional patterned
MgO substrates
~ fabrication of FZO nanowire structure~

## Slide 2: Contents
Introduction of keyword
  3d transition metal oxide & FZO
  Magnetic domain and magnetic domain wall
  Constricted ferromagnetic nanowire structure
  Nano processing procedure for metal oxides
My research
  Sidewall growth method & Fabrication process
  Anneal condition
  Three dimension MgO nanowire structure
  Structure analysis by TEM
  MgO growth mechanism
Conclusion

## Slide 3: Contents
Introduction of keyword
  3d transition metal oxide & FZO
  Magnetic domain and magnetic domain wall
  Constricted ferromagnetic nanowire structure
  Nano processing procedure for metal oxides
My research
  Sidewall growth method & Fabrication process
  Anneal condition
  Three dimension MgO nanowire structure
  Structure analysis by TEM
  MgO growth mechanism
Conclusion

## Slide 4: 3d transition metal oxide(3d遷移金属酸化物)
Ferroelectric
BaTiO3
science 303 661(2004)
Ti
Ni
V
Co
Cr
Mn
Fe
Cu
Metal-Insulator
transition
VO2
Thin solid films 486 46(2005)
Ferromagnetic
Fe3O4,Fe3-xZnxO4
small 4 1661(2008)
High temperature
superconduction
YBa2Cu3O7
PRL. 58 1574(1987)
Strongly-correlated electron system Variety of function
（強相関電子系）
Fe3+
O2-
Fe2+
Spinel structure
Ferromagnetic at roomtemperature
and high spin polarization
Control of carrier concentrate
Enviromental friendly material
（環境調和型材料）
Clark number
O : (49.5) 1
Fe : (4.70) 4
PRB. 76 205108(2007)
PRB. 76 205108(2007)
O
Zn
Fe
Fe3-xZnxO4(FZO)
O
Si
Fe
Al

## Slide 5: Ferromagnetic nanostructures
Fe3-xMnxO4-nanowire MFM image
Nano Lett. 9 1962(2009)
Average of
non-uniform magnetic
Nonconventional giant
nonlinearly response
Magnetic
domain
Magnitic
domain
wall
Magnetic
domain
~50nm
~70nm
100nm
50nm
Magnetic domain
➞Field of one direction of magnetic moment
Magnetic Domain wall
➞Field of rotation spin among magnetic domain
（磁区）
（磁壁）
Pinning domain wall
Applied Physics Express 4 (2011) 033001
application
Current-driven domain wall motion
in a magnetic constricted nanowire
Merit
Nonvolatile
High speed
High integration
Low consumed power
Unlimitedly write
Unlimitedly read
応用物理 79 1071(2010)

## Slide 6: Nano processing procedure for metal oxides
Oxide has high physical hardness and chemical stability.
It is diffcult to fabricate a few dozen nanometer patterns.
Nano Lett. 9 1962(2009)
JJAP. 42 6721(2003)
Photo lithography
EB lithography
FIB lithography
AFM lithography
APL. 89 122101(2006)
APL. 84 5213(2004)
Top down
TiO2
MoO3
Cu2O3
LaAlO3
Appl. Surf. Sci. 253 1758(2006)
Superlattice Microst 46 513(2009)
Pulse laser
deposition
chemical vapor
deposition
Bottom up
ZnO
ZnO

## Slide 7: Contents
Introduction of keyword
  3d transition metal oxide & FZO
  Magnetic domain and magnetic domain wall
  Constricted ferromagnetic nanowire structure
  Nano processing procedure for metal oxides
My research
  Sidewall growth method & Fabrication process
  Anneal condition
  Three dimension MgO nanowire structure
  Structure analysis by TEM
  MgO growth mechanism
Conclusion

## Slide 8: Combination method
Nanoimprint(NIL)
High processing accuracy of side surface
Control of position and shape
Pulse laser deposition(PLD)
Deposition of thin film from atomic layer
The most suitable method to fabricate thin film of oxide
substrate
Excimer laser
Fabrication of highly ordered nanopattern structures
  Deposition time and angle
  ➞Control of width
  Shape of substrate
  ➞Control of shape and height of oxide structure
~10nm

## Slide 9: Purpose
substrate
substrate
Anneal condition of MgO crystalization
Structure analysis by TEM
MgO nanowire growth mechanism
Fabrication of highly ordered nanowire structures

## Slide 10: Fabrication process
MgO substrate
MgO substrate
MgO substrate
MgO substrate
MgO substrate
Three dimension MgO nanowire
FZO nanowire
①cleaning substrate
②nanoimprint
③PLD（MgO）
④removing resist
⑤annealing
resist
MgO
MgO substrate
⑥PLD(FZO)&ECR
FZO
MgO substrate
⑦removing MgO
＜a few dozen nm

## Slide 11: MgO crystallization condition by postanneal
STO(002)
STO(003)
MgO(022)
MgO was crystallized by postannealing at 1000℃
STO substrate
STO substrate
MgO

## Slide 12: Anisotropy growth of MgO nanowire
Schematic diagram
[100]
[010]
substrate
500nm
Zig-Zag line
MgO(001)nanowire
MgO(001)substrate
[100]
[010]
500nm
[100]
[010]
Parallel line
MgO(001)substrate
MgO(001)nanowire
[001]
[001]
MgOsubstrate
MgOnanowire
[100]
[010]
MgOsubstrate
MgOnanowire
[100]
[010]
[001]
[001]
300nm
MgOnanowire
MgO(001)substrate
[100]
[010]
[001]
After anneal (1000℃)
Before anneal
MgO(001)substrate
MgOnanowire
300nm
[001]
[100]
[010]

## Slide 13: Structure analysis of MgO nanowire (TEM)
200nm
MgOsubstrate
MgOnanowire
MgOsubstrate
MgOnanowire
10nm
MgO nanowire(TEM)
MgO substrate(TEM)
I confirmed that quality of crystallized MgO nanowires is similar to MgO substrates. MgO grows so that MgOnanowire(001)[100]//MgOsubstrate(001)[100].
2nm
2nm
MgO nanowire(FFT)
MgO substrate(FFT)
Fracture
direction
[110]

## Slide 14: MgO growth mechanism
[100]
[010]
substrate
500nm
Zig-Zag line
MgO(001)nanowire
MgO(001)substrate
[100]
[010]
500nm
[100]
[010]
Flatness line
MgO(001)substrate
MgO(001)nanowire
I confirmed that MgO(110) appears in side surface of MgO nanowire.
Growth
mechanism
MgO nanowire
MgO nanowire
[110]
[110]
[100]
[010]
[100]
[010]
[001]
[001]
[001]
[001]

## Slide 15: Conclusion
I tried to fabricate the three dimension MgO nanowire structures.
I confirmed that MgO was crystallized by postannealing at 1000℃.
I confirmed that quality of crystallized MgO nanowires is similar to MgO substrates.
I confirmed MgO growth mechanism by TEM.
I succeed in fabrication of the MgO nanowires structure with flat MgO(110) side surface.
I have been trying to fabricate FZO nanowire structures on the 3D MgO nanowire substrate, and study their magnetic properties.
Future plane