## Slide 1: Direct conversion of graphite into diamond through electronic excited states
H.Nakayama and H.Katayama-Yoshida
(J.Phys : Condens. Matter 15 R1077 (2003)
Yoshida Lab.
Presenter: Sho Nishida

## Slide 2: Contents
Introduction
・Ultrahard material
・Polymorphism of Carbon
First principles calculations
Graphite Diamond conversion
・Applying pressure
・Hole doping
Theoretical prediction of a new diamond synthesis method
Summary
Polymorphism : 結晶多形

## Slide 3: Mohs hardness
タルク、滑石
Japanese name
石こう、ジプサム
ホタル石
方解石、カルサイト
リン灰石
正長石、長石
石英、クォーツ
トパーズ
コランダム
ダイアモンド
Talc
Mineral
Gypsum
Fluorite
Calcite
Apatite
Orthoclase Feldspar
Quartz
Topaz
Corundum
Diamond
Mohs hardness
1
2
4
3
5
6
7
8
9
10

## Slide 4: Ultrahard materials
Diamond
・Diamond can resist indentation pressures of 97 GPa.
Hexagonal diamond (Lonsdaleite)
・Lonsdaleite can resist indentation pressures of 152 GPa.
(by using ab-initio calculation[1])
W-BN (Wurtzite Boron Nitride)
・W-BN can resist indentation pressures of 114 GPa.
(by using ab-initio calculatiuon[1])
[1] Z.Pan, H,Sun et al Phys.Rev.Lett. 102, 055503 (2009).
ab-initio calculation:第一原理計算

## Slide 5: Polymorphism of Carbon
(a). hexagonal graphite
(b). rhombohedral graphite
(c). simple hexagonal graphite
(d). cubic diamond
(e). hexagonal diamond
Polymorphism : 結晶多形

## Slide 6: Hexagonal graphite (AB stacking)
・Half of the atoms are directly located just above each other in adjacent planes.
・the other half are directly above the centers of the hexagonal rings in the adjacent plane.
B layer
A layer
A layer
B layer

## Slide 7: Rhombohedral graphite (ABC stacking)
・Half of the atoms are directly above atoms in the adjacent plane and directly below the centers of the hexagonal rings.
・the other half are directly below atoms and above the ring centers.
A layer
B layer
C layer
A layer
B layer

## Slide 8: Simple hexagonal graphite (AA stacking)
・All atoms are directly above each other
in the adjacent planes
A layer
A layer
A layer

## Slide 9: Cubic diamond
・Atomic position
in the unit cell is that
( 0 0 0)
( ¼ ¼ ¼)
Lattice parameter = 3.56 Å
Energy gap = 5.47 (eV)

## Slide 10: Hexagonal diamond (Lonsdaleite)
・Lonsdaleite is obtained
from simple hexagonal graphite
by decreasing the interlayer
distance and
by buckling the hexagonal rings.
Lonsdaleite：ロンズデーライト

## Slide 11: First principles calculations
Veff(r)
ψi(r)
?
DFT(Density Functional Theory)

## Slide 12: First principles calculations
Based on DFT ( Density Functional Theory)
Exchanged correlation energy term
・LDA (Local Density Approximation)
・GGA (Generalized gradient approximation)
Basis function
・Plane Wave basis
・Local Orbital basis (Gaussian basis,etc)
Treatment of core electron
・All electron
・Pseudo potential
Pseudo-potential：擬ポテンシャル
FLAPW (Full potential linearized augmented planewave method)

## Slide 13: Graphite-to-diamond transition
・The transition from rhombohedral graphite to
cubic diamond can be investigated
by calculating the total energy E (V,β,γ)
as a function of V, β(=c/a), γ(=R/c).
V is cell volume,
R is length between the first atom and
the second atom.

## Slide 14: Rhombohedral structure
α
α
α
ｃ
a
ｂ
a

## Slide 15: c/a , R/c
a
C
a
R

## Slide 16: The structure of the rhombohedral graphite
When R/c=1/3,
The rhombohedral graphite structure is realized
R
C

## Slide 17: The structure of cubic diamond
When R/c=1/4,
The cubic diamond structure is realized

## Slide 18: Total energy dependence on the applied pressure
・the graphite phase becomes
unstable with an increase of
the applied pressure.
・In 0 Pa, the activation energy
is found to be 0.29eV/atom
High pressures is necessary to cause transition into the diamond
in the ground state.

## Slide 19: The total energy for the hole doped state
The activation energy vanishes
at the concentrations of
more than nh = 0.125[1/atom]
Doping holes induce a similar effect as applying pressure.

## Slide 20: Theoretical prediction of a new diamond synthesis method
The graphite structure is unstable in the hole-doped state.
When graphite is excited with SR x-ray,
a hole is created at the C 1s core level.
Through Auger decay process,
The hole is created in the valence band.
The conversion into diamond can occur

## Slide 21: Auger decay process
electron
hole
Conduction Band
Valence Band
Core Level
Vacuum

## Slide 22: Schematics of graphite – diamond transition
sp2 hybrids
(σ-bond)
Π-bond
p orbital
sp3 hybrids
Diamond
Graphite

## Slide 23: The advantages of this synthesis method
・no impurities
・Transition can proceed even at room temperature
・Size of the crystal is controllable
by tuning the irradiated areas and the intensity of the SR x-ray

## Slide 24: Summary
When holes are excited in the valence π band,
The configuration in the graphite structure
becomes markedly unstable.
SR x-ray can induce the conversion into diamond through the Auger decay process.

## Slide 25
Fin