## Slide 1
Fe
As
Nodal superconducting gap structure in superconductor BaFe2(As0.7P0.3)2
M-colloquium
5th October, 2011
Dulguun Tsendsuren
Kitaoka Lab.
Division of Frontier Materials Sc.
Department of Materials Engineering Sc. Graduate School of Engineering Sc., Osaka Univ.
Y. Zhang et al., Fudan Univ., Shanghai, China, arXiv:1109.0229v1

## Slide 2: Contents
1
Introduction
  Brief intro to Superconductivity 超伝導
  Superconducting gaps 超伝導ギャップ
  Experimental method for probing SC gap: ARPES
    Angle Resolved Photo Emission Spectrum 角度分解型光電子分光
Exp. result for BaFe2(As0.7P0.3)2, by ARPES
  Fermi Surfaces フェルミー面
  Superconducting gap超伝導ギャップ
Summary
Introduction

## Slide 3: What is Superconductivity?
Introduction
If substance is in superconducting state, which:
  Has no electric resistance 電気抵抗
  Repels magnetic field 磁場 from itself
2

## Slide 4: Iron-based SC 鉄系超伝導: Ba122
0
T [K]
SC
Ba1-xKxFe2As2
( Tc=38K)
hole-doping
AFM
x
Full gap
KFe2As2
Tc=38K
Ba2＋→K+
Ba/K
Ba0.6K0.4Fe2As2
Full gap
Ba
BaFe2(As0.66P0.33)2
As3-→P3-
Nodal
Tc=30K
a = 3.92 Å
c ~ 12.8 Å
hPn~1.32 Å
Matsuda group,
Ishida group
a ~ 3.92 Å
c ~ 13.3 Å
hPn~1.38 Å
Optimum height
Rotter et al. (2008)
BaK122
Ba122P
y
BaFe2(As1-yPy)2
isovalent-doping
SC
( Tc=30K)
Nodal
Introduction
3
What is
superconducting gap?
Notes: Shrinks only through c-axis. In each cases, a is constant.

## Slide 5
Introduction
Superconducting gap
Energy
EFermi
Full
Density of State
gap
Density of State
Energy
EFermi
Nodal
gap
4
SC gap appears in low temperature ( < Tc 転移温度) at the same time with SC state, due to coupled electrons 電子対 (cooper pair クーパー対)
How to distinguish this two?
What about iron-based superconductors?
Interaction energy 相互作用のエネルギー: ≈10-3[eV]
Interaction distance 相互作用の距離: > 100[nm]
BCS superconductors
High Tc cuprate superconductors

## Slide 6
Introduction
Possible SC order秩序 parameters
and their spin-stateスピン状態
BCS SC
High-Tc oxides
CeCu2Si2 UPd2Al3, CeRIn5
UPt3 Sr2RuO4
5

## Slide 7
Introduction
SC gap in iron-based SC
Structure | Substance
122 | Ba1-xFe2-xCoxAs2
122 | Ba1-xKxFe2As2
122 | KxFe2-xSe2
11 | FeTe1-xSex
Structure | Substance
11 | FeSe
111 | LiFeP
1111 | LaOFeP
122 | KFe2As2
122 | BaFe2-xRuxAs2
122 | BaFe2(As1-xPx)2
Energy
EFermi
Full
Density of State
gap
Density of State
Energy
EFermi
Nodal
gap
NMR, Penetration Depth,
Thermal Conductivity,
Scan tunneling spectroscopy
6
Node position in FSs?

## Slide 8
Introduction
ARPES
7
Based on Photoelectric effect 光電効果
Measures an intensity of released electron energy
  More intensity ⇒ More occupied states占有状態
  Less intensity ⇒ Less occupied states占有状態
In this manner, directly measures DOS状態密度!!!
FSs can be drawn by angle resolved method

## Slide 9
Exp. results
BaFe2(As0.7P0.3)2
8
Zero resistivity
Meissner effect

## Slide 10
Exp. results
Phase diagram相図
9
BaFe2(As1-xPx)2
Tc = 30[K] (x = 0.3)
Fe
As
hPn:
Distance between
Fe layer and As

## Slide 11
Exp. results
ARPES result on BaFe2(As0.7P0.3)2
Z. R. Ye et al., arXiv: 1105.5242v1
BaFe2(As0.7P0.3)2
Ba0.6K0.4Fe2As2
10

## Slide 12
3D view
Exp. results
ARPES result on BaFe2(As0.7P0.3)2
BaFe2(As0.7P0.3)2
Z. R. Ye et al., arXiv: 1105.5242v1
11

## Slide 13
Exp. results
12
BaFe2(As0.7P0.3)2: Hole pocket
at 9[K]

## Slide 14
Exp. results
BaFe2(As0.7P0.3)2: Electron pocket
13
at 9[K]

## Slide 15
Exp. results
Temperature dependence of gap
Hole pocketsホール面
14

## Slide 16
Exp. results
Electron pockets電子面
15
Temperature dependence of gap

## Slide 17
Exp. results
ARPES results on BaFe2(As1-xPx)2
16
in Electron pockets電子面
Hole pocketsホール面
no Nodes
Node exists on

## Slide 18
Exp. results
ARPES results on BaFe2(As1-xPx)2
3D-like FSs around ГZ axis
At Z point, α surface has no energy gap
From ARPES:
SC (line) nodal gap exists
17

## Slide 19
Summary I
18
Type | Pocket | SC gap
Hole | α | Nodal
Hole | β | Full
Hole | γ | Full
Electron | δ | Full
Electron | η | Full
Superconducting gap
of each pocket
Nodal gap
α band mixes with
α and β : δ
γ : η
Nesting between
Γ and M
ARPES results on BaFe2(As1-xPx)2

## Slide 20
As pnictogen height becomes lower, FSs become 3D like.
Even 3D like FSs cause large RDOS, Tc is still high enough.
Multiband effect
BaK122
Ba122P
Sr122P
Suzuki, Usui, Kuroki et al., JPSJ(2011)
Y. Zhang et al., arXiv: 1109.0229v1
10
Summary II
Comparison with Theory
19

## Slide 21
Conclusions in this work
Thank you for your attention
The End
This work unifies the seemingly diversified phenomenology of nodal and nodeless superconducting gaps in various iron based superconductors,
and
It provides a discriminator for theories on iron pnictides.