## Slide 1: Magnetic-field-induced charge-stripe order in the high-temperature superconductor YBa2Cu3Oy
Tao Wu et. al.
Nature 477, 191 (2011).
Kitaoka Lab.
Takuya Kaneda
1

## Slide 2: CONTENTS
Introduction
  Phase Diagram of Copper Oxides
  Variation of YBa2Cu3Oy
  Fermi Surface of Copper Oxides
Experimental Result
  63Cu-NMR Spectra
  Charge-Stripe Order
  Phase Diagram
Summary
2

## Slide 3
Introduction

## Slide 4
Phase Diagram of Copper Oxides
Introduction
※AFM = Anti-ferromagnetism （反強磁性）
Phase Diagram
of Copper Oxide Superconductors
Hole concentration: p
Carrier concentration is an important parameter.
When p = 0,
  copper oxides show AFM.
As p is increasing,
  AFM phase disappears.
  SC phase appears.
Tc depends on p.
3

## Slide 5
 | YBa2Cu3O6 | YBa2Cu3O6.5 | YBa2Cu3O7
Structure |  |  | 
Conductivity | Mott Insulator | Superconductor (under-doped) | Superconductor (optimally doped)
Critical Temperature | × | Tc = 60K | Tc = 90K
Hole Concentration | p = 0 | p ~ 0.1 | p ~ 0.194
Fermi Surface |  |  | 
Variation of YBa2Cu3Ox
Introduction
4

## Slide 6
Hole concentration: p
Fermi Surface of Copper Oxides #1
ARPES Result （角度分解光電子分光法）
From band theory,
the large Fermi surface had been predicted.
in fact…
Tl2201
N. Doiron-Leyraud et al., Nature 447, 565 (2007).
※ ARPES = Angle Resolved PhotoEmission Spectroscopy
Introduction
5

## Slide 7
Hole concentration: p
Fermi Surface of Copper Oxides #2
ARPES for underdoped copper oxide
fermi arc
In high magnetic field (~30T),
Fermi pocket (red eclipse) was suggested !
In 2007 , quantum oscillation was observed in YBCO.
Direct proving for Fermi surface!
※ quantum oscillation （量子振動, ド・ハース振動） 低温, 高磁場, 綺麗な試料が必要。
Fermi pocket
Introduction
Na-CCOC
Shen et al., Science 307, 901 (2005).
6

## Slide 8
By changing the hole concentration p,
what happend?
Fermi pocket
7
Question

## Slide 9
New Brillouin zone !
underdope
folding
overdope
2a
a
Fermi Surface Reconstruction
any translational symmetry breaking?
(spin and/or charge order ? )
Introduction
並進対称性の破れ
8

## Slide 10
Magnetic-field-induced AFM order of LSCO
B.Lake et al.,
Nature 415, 299-302 (17 January 2002)
La1.9Sr0.1CuO4 (LSCO)
AFM ordering
Such ordering occurs in YBCO as well ?
9

## Slide 11
Experiment

## Slide 12
63Cu-NMR
63Cu: Spin I = 3/2 (1)
Quadrupole Interaction （電気四重極相互作用）
(interaction between quadrupole moment and electrical gradient)
Two satellite peaks are also observed!
Experiment
10

## Slide 13
Samples
YBa2Cu3O6.54 (p = 0.108)
YBa2Cu3O6.67 (p = 0.12)
ZOOM
Cu2F is located below Oxygen-Filled chain.
Cu2E is located below Oxygen-Empty chain.
Experiment
Tc = 61.3K
Tc = 66.0K
11

## Slide 14
63Cu-NMR Spectra (H = 15T)
central
satellite
satellite
No temperature dependence at H = 15T
frequency (MHz)
Cu2E
Cu2F
Experiment
12

## Slide 15
2E
2E
2E
2E
2E
63Cu-NMR Spectra (H = 28.5T)
central
satellite
satellite
Cu2F peaks are splitting!
Knight Shift
νQ
Between Cu2Fa and Cu2Fb,
local environment is different.
Experiment
59K
1.3K
2F
2Fa
2Fb
(νQ =30.47MHｚ)
(νQ =30.7MHｚ)
(νQ =30.37MHｚ)
13

## Slide 16
No broadening of spectrum
Spin order is absent.
63Cu-NMR Spectra
Experiment
central
satellite
satellite
H = 15T
H = 28.5T
14

## Slide 17
Charge-Stripe Order
YBCO (p = 0.108)
Fermi surface reconstruction
Experiment
2Fa
2E
2Fb
2E
2Fa
2E
p0 = 0.108
Δp = 0.03
15

## Slide 18
Phase Diagram of YBa2Cu3Ox
TN (antiferromagnetic order)
Tcharge (charge order)
T0 (Fermi surface reconstruc-
tion)
※ T0 is defined as the temperature where the Fermi surface reconstruction occurs.
(Hall coefficient RH measurement)
Tcharge coincides with T0.
Charge-stripe order is related to the Fermi surface reconstruction.
AFM
16

## Slide 19: Summary
They carried out 63Cu-NMR to reveal any ordered state.
High magnetic field induces the charge-stripe order instead of spin order.
Fermi surface reconstruction is probably associated with the charge-stripe order because T0 coincides Tcharge.
17

## Slide 20
Thank you for your attention.
18