## Slide 1: Pressure effect on electrical conductivity of Mott insulator “Ba2IrO4”
Shimizu lab. ORII Daisuke

## Slide 2: Contents
Introduction : H. Okabe et al., Phys. Rev. B 83, 155118(2011)
Mott insulator
Ba2IrO4 Mottness
Structure
Magnetic property
High-pressure effect
Motivation
Research
Summary

## Slide 3: Mott insulator
E
E
Introduction
EF
large
On-site coulomb interaction U
Metal
Kitaoka-sensei’s lecture
U

## Slide 4: Ba2IrO4 : Mottness
Introduction
Iridium 5d5
eg
t2g
Crystal field
SO coupling
5d
Insulator ??
Metal??
B. J. Kim et al., PRL 101, 076402 (2008)
E
EF
E
EF

## Slide 5: Ba2IrO4 : structure
Same structure with high-Tc materials
Ex.) Sr-La-Cu-O, Ba-La-Cu-O, etc…
2 dimensionality
The effect of
spin fluctuation
strongly appears.
Introduction
The interaction is weaker for lower dimension.
Flat IrO2 square

## Slide 6: Ba2IrO4 : magnetic property
Spin fluctuation
Both oh the magnetic moments are reduced by the spin fluctuation.
Antiferromagnetic order
Neel temperature TN is similar.
 | Magnetic moment (at low temperature) | TN
Ba2IrO4 | 0.34 μB/Ir atom | 240 K
La2CuO4 | 0.40 μB/Cu atom | 220 K
D. Vaknin et al., Phys. Rev. Lett. 58, 2802 (1987)
Ba2IrO4 will be superconductor…?
Introduction
Ba2IrO4
La2CuO4
compare

## Slide 7: High-pressure effect
Pressure
Electronic states change!
Transitions
Structural transition
Magnetic transition
M-I transition
etc…
I’m particularly interested in
superconducting transition.
Introduction

## Slide 8: Motivation
It is expected that
superconductivity will be observed
in Ba2IrO4.

## Slide 9: How to make high pressure
Measurement
Electrical resistance;
4-terminal method
Pressure
Ruby fluorescence method
Temperature
Research
V+
V-
I+
I-

## Slide 10: Result
Research
Metallic behavior
12~23GPa Insulator behavior
~10K

## Slide 11: Discussion
M-I transition
Research
But the superconductivity phase was not observed down to 10K.
E
E
?
H. Okabe et al., Phys. Rev. B 84, 115127 (2011)

## Slide 12: Summary
M-I transition was observed at 25 GPa.
But superconductivity was not observed.