## Slide 1
Dynamics and Mechanisms of
the Multiphoton Gated Photochromic Reaction
of the Highly Fluorescent Diarylethene Derivatives
Miyasaka Lab
Kunishi Tomohiro

## Slide 2
Contents
Introduction
  The definition of the Photochromism
  Application and Conditions required for
  the photochromic molicules in the application
  The highly fluorescent Diarylethene derivative
Results & Discussion
  The dynamics of the excited state
Summary
  The prospect for the future

## Slide 3
Photochromism
the reversible photoinduced isomerization reactions
between two isomers
UV light
Vis. light
Example (Diarylethene in solution)
Introduction
Open form
Closed form
1

## Slide 4
Application of Photochoromic Molecules
Introduction
Quick property change
Absoption spectra
Refractive indices
Redox potential
etc.
Photo-electronic devices
  Photo-memories
  Photo-switches etc.
Fluorescent dyes
for super-resolution microscopy
Application
2

## Slide 5
Conditions required the Photochromic Systems toward the
Actual Application(memories and switchable fluorescent dyes)
Introduction
Thermal stability of both isomers
Low fatigue
<memory>
The colored state should keep its color while it is written in the memory
<switchable fluorescent dyes>
The fluorescent emission should be kept when the molecule is in the ON state of the fluorescence
3
S1
hn
Colorless
(OFF) state
Colored (ON )state
fluoresence
The gated function with the light intensity
by using multiphoton absorption process
But nondestructive performance is in conflict with the non-destructive
performance for the switchable molecular systems.
Rapid response
High sensitivity
Non-destructive performance

## Slide 6
Diarylethene derivative
(highly fluorescent)
Open form
Closed form
Absorption spectra
Open form in 1,4-dioxane
(Black dashed line)
Closed form in 1,4-dioxane
(black solid line)
Fluorescence spectra
Closed form under irradiation
with 532 nm light
(red line)
(M. Irie,et al, J. Am. Chem. Soc. 2011,13558.)
Results & Discussion
Φ=0.21
Φ<10-5
4
(non-fluorescent)
ΦF~0
ΦF=0.78

## Slide 7
Diarylethene derivative
Fluorescence time profile
Closed form under irradiation
with 532 nm light
fluorescence lifetime = 2.6 ns
(M. Irie,et al, J. Am. Chem. Soc. 2011,13558.)
(highly fluorescent)
Open form
Closed form
Φ=0.21
Φ<10-5
Results & Discussion
5
(non-fluorescent)
ΦF~0
ΦF=0.78

## Slide 8
Observation of Reaction Dynamics
by Trasient Absorption Spectroscopy
Dt
sample
photo detector
pump pulse (532 nm)
monitor pulse (white light)
Trasient absorption spectroscopy
Open form
Closed form
Results & Discussion
Drastic enhancement of reaction yield
6
ca.10 %
← Ground state of Closed form
← Excited state of Closed form

## Slide 9
Excitation intensity dependence : conversion efficiency at 20 ns after the excitation with a 15-ps 532-nm laser pulse.
Conversion Efficiency
-DAbs510nm / Abs510nm
Conversion efficiency is
quadratically in proportion
with the excitation intensity
Two-photon process is responsible for
the efficient bond breakage.
Conversion efficiency:変換効率
Results & Discussion
slope~2
7

## Slide 10
Two-Photon Absorption Processes
Sn
S0
hv
hv
S1
S0
hv
hv
Simultaneous two-photon absorption process
Stepwise two-photon absorption process
Re-absorption of intermediate species
The competition of absorption of light
between the ground state molecule and the intermediate species.
Effective in the case where the number of total photon is large.
I ：Peak Intensity (photon / cm2 sec)
δ : 2-photon absorption cross section
Ng : the number of the ground-state molecules
Ne : the number of the excited state molecules
Simultaneous two-photon absorption :同時二光子吸収
Stepwise two-photon absorption :逐次二光子吸収
Results & Discussion
8

## Slide 11
Comparison of Picosecond and Femtosecond
Lasers
Laser | Wave length | Pulse Duration (fwhm) | Peak Intensity (I) | Total photon number | Drastic Enhancement of the apparent reaction yield
PS | 532 nm | 15 ps | small | large | ○
FS | 540 ~ 610 nm | 150 fs | large | small | ×
Results & Discussion
9
Stepwise two-photon absorption process

## Slide 12
Excitation intensity dependence : conversion efficiency at 20 ns after the excitation with a 15-ps 532-nm laser pulse.
Conversion efficiency:変換効率
Results & Discussion
90 %
10 %
≈0 %
hv
hv
closed form
open form
Sn
S1
S0
10

## Slide 13
Future prospect
Results & Discussion
Super-resolution fluorescence imaging
Stefan W. Hell, et al, Science, 316 (2007) 1153.
11

## Slide 14
Super-resolution microscopy (PALM)
12
Stochastically ON
(one-photon absorption)
hv
(activation)
Analysis of the center
of the lighting spot
Perfect OFF
(Two-Photon Absorption)
VIS
(short pulse)
repeatedly
We can get the good image
more efficiently.

## Slide 15
Summary
Picosecond pulsed excitation of the closed-isomer of the
diarylethene derivatives led to the drastic enhancement of the
cycloreversion reaction. (Φ<1.0×10⁻⁵→1.0×10⁻1)
This enhancement is attributable to the production of the higher
excited state with a large reaction yield of the cycloreversion
(ca.10%) attained via a successive two-photon process.
Two-photon gated reaction in opening reaction can be utilized to
the deterministic switching ,which can be applied to
the super-resolution fluorescence imaging.
13
Thank you for your attention