## Slide 1: Controlling the thickness of CuCl thin films and improving their quality by means of MBE method
Ashida lab. M1 Kamizono Kenta

## Slide 2
Introduction
  All-optical switching devices
  Excitons and light in the high-quality system
Background
Previous results
  Temperature dependence of DFWM spectrum
Purpose
Experimental results
Summary
Contents
DFWM(Degenerated Four Wave Mixing):縮退四光波混合

## Slide 3
All-optical switching devices
all-optical information processing
superior performances than electronic communication devices
  transmission rate 伝送効率
  energy efficiency エネルギー効率
Introduction
All-optical switching devices 光スイッチ
Realization
by nonlinear optical effect
非線形光学効果
Optical switching device
Transient grating
過渡回折格子
Probe pulse
Pump pulses
Signals

## Slide 4
Exciton
Trade-off problem
high efficient response 高効率応答
available in the micro crystal
Introduction
Exciton and trade-off problem
Low consumption energy
低消費エネルギー
resonance between light and excitons
High response speed 高速応答
nonresonance between light and excitons
+
-
Means of confining excitons in the micro crystal
can break down this problem.

## Slide 5
Spatial interplay between waves of excitons and light
Nanostructure
Long wavelength approximation (LWA) regime 長波長近似領域
size << wavelength of light
dominant interplay between the exciton of lowest state and light
Oscillator strength increases with the system size.
Dependence of the exciton radiative decay time in CuCl microcrystals
n = 1
Exciton
Light
n = 2
n = 4
n = 3
Ref: T. Itoh, M. Furumiya, and T. Ikehara, Solid State Commun. 73, 271 (1990).
over LWA
Introduction

## Slide 6
Excitons and light in the high-quality system
System where exciton wave functions are coherently extended to the whole volume
Ultrafast response
beyond LWA regime
Nanostructure
LWA regime
Coupling of multinode-type excitons with light
The coupling with the size increase is not limited.
n = 1
Exciton
Light
n = 2
n = 4
n = 3
Exciton
Light
Introduction

## Slide 7
Uncoupled excitonic modes
Eigenenergy including the radiative shift
Radiative width:Γn
Real part of radiative corrections
Imaginary part of radiative corrections
τ :radiative decay time
τ = ħ/2Γn
Radiative corrections (輻射補正)
in the coupled system of photons and excitons
Ref: H. Ishihara, J. Kishimoto and K. Sugihara, J. Lumin. 108, 343 (2004).
Size dependence of radiative corrections for the CuCl Z3 exciton (theory)
Introduction
330 nm

## Slide 8
large exciton binding energy (200 meV)
small exciton Boar radiance （0.7 nm)
The center-of-mass confined effect of excitons is available.
Cu+
Cl-
Zinc Blend
E
ｋ
Z3
Z1,2
direct transition semiconductor
Property of CuCl
Suitable material
for research of the center-of-mass confined effect of excitons
Background

## Slide 9
AFM image of CuCl thin film
AFM image of high-quality CuCl thin film (by RHEED)
CaF2 cap layer
40 nm
CaF2(111) substrate
CaF2 buffer layer
CuCl layer
40 nm
1 mm
e-beam-exposed
Growth of high-quality CuCl thin films
Surface morphology is extremely improved by electron beam irradiation.
 | Lattice constant
CaF2 | 0.5463 nm
CuCl | 0.5406 nm
Atomic Force Microscope ; AFM
Background

## Slide 10
Eigenenergy including the radiative shift
Radiative width
261 nm
k1
k2
2k1ｰ k2
2k2ｰ k1
Degenerated Four Wave Mixing（DFWM）
Mode structures of DFWM spectrum
in a high-quality CuCl thin film
M. Ichimiya, M. Ashida, H. Yasuda, H. Ishihara, and T. Itoh, Phys. Rev. Lett. 103, 257401 (2009)
Previous results
Several peak structures appear.
Good agreement with eigenenergy including the radiative shift

## Slide 11
Previous results
Temperature dependence of DFWM spectrum (68 nm)
Both spectral dependences are same.
A component for n=2 becomes dominant as the temperature increases.
0.29
5.0
1.8
n = 3
n = 2
n = 1
Radiative width (meV)
Calculated induced
polarization spectra
DFWM spectra
The excitonic state with the largest radiative width may be observed at high temperatures.

## Slide 12
Spectral shape changes as temperature increases.
Components with smaller radiative width disappear at lower temperatures.
A component for n = 5 becomes dominant and only the state is observed above 210 K.
Previous results
Temperature dependence of DFWM spectrum (310 nm)
M. Ichimiya, K. Mochizuki, M. Ashida, H Yasuda, H. Ishihara, and T. Itoh, Phys. Status Solidi B 248, 456–459 (2011)
0.27
0.46
1.4
n = 8
n = 7
n = 6
Radiative width (meV)
n = 5
19
DFWM signal can be observed
at room temperature!

## Slide 13
Deciding the condition of fabricating CuCl thin film by means of molecular beam epitaxy (MBE) method (329nm)
Fabricating high-quality CuCl thin film on improving the quality
Purpose
Realizing ultrafast radiative decay by the curtain thickness on large radiative width
Enhancement of DFWM signal on improving the quality of CuCl thin film
Realization of efficient and ultrafast
radiative decay above room temperature
Light
Exciton
Light
Exciton
High-quality

## Slide 14
melting pot
substrate
screen
RHEED
shutter
shutter
pump
oscillator crystal
CaF2
CuCl
K-cell
Experimental Procedure
Vacuum
1.0×10-6 ～ 9.0×10-7 Pa
CaF2(111) substrate
CaF2 buffer lay
CuCl layer
40 nm
1 mm
329 nm
CuCl layer
substrate temperature
: 50~150 0C
growth rate: 0.13 nm/s
CaF2 buffer layer
substrate temperature
: 600 0C
growth rate : 0.02 nm/s
Molecular Beam Epitaxy (MBE) method

## Slide 15
results
Transmission of normal incident light
in the transparent region (150 ℃)
 | crystal oscillator |  | measured thickness |  | substrate temperature
’10 12/09 | 150nm |  | ×2.0 | 300nm | 150℃
‘10 12/23 | 162nm |  | ×1.9 | 309nm | 150℃
‘11 01/13 | 172nm |  | ×1.8 | 314nm | 150℃
  The difference is not same.
Lower substrate temperature
CuCl evaporate
on the substrate again.
Light
L
n = 1
n = 2

## Slide 16
results
 | crystal oscillator |  | measured thickness |  | substrate temperature
’11 02/20 | 172nm |  | ×1.7 | 293nm | 80℃
‘11 02/24 | 172nm |  | ×1.7 | 290nm | 130℃
The differences are same at lower substrate temperature.
What quality does the CuCl thin film have
Transmission of normal incident light
in the transparent region (130 ℃)
Light
L
n = 1
n = 2

## Slide 17
AFM image (150℃)
results
 | crystal oscillator |  | measured thickness |  | substrate temperature
‘10 12/23 | 162nm |  | ×1.9 | 309nm | 150℃
’11 01/13 | 172nm |  | ×1.8 | 314nm | 150℃
’10 12/23
20 nm
3 μm
’11 01/13
20 nm
3 μm
Surface morphology is extremely-good.

## Slide 18
AFM image (under 130℃)
results
’11 02/24
20 nm
3 μm
’11 02/20
20 nm
3 μm
 | crystal oscillator |  | measured thickness |  | substrate temperature
’11 02/20 | 172nm |  | ×1.7 | 293nm | 80℃
‘11 02/24 | 172nm |  | ×1.7 | 290nm | 130℃
Surface morphology is extremely-good.
Which is better,
high substrate temperature or low?

## Slide 19
Mode-locked
Ti:sapphire laser
Cryostat(6K)
CCD
Pulse width:110 fs
Repetition:80 MHz
wavelength：387nm
Monochro-
mator
Sample (CuCl)
SHG crystal
BS
Optical fiber
Degenerated Four Wave Mixing (DFWM) spectroscopy
Experimental configuration

## Slide 20
Photon energy of each peak is in good agreement.
Sharp peak structures appear.
DFWM spectrum in high-quality CuCl thin film (150℃)
results
 | measured thickness | substrate temperature
’11 01/13 | 313nm | 150℃
High-quality
CuCl thin film
Thickness
313nm
6K
313 nm

## Slide 21
DFWM spectrum depends on the thickness of CuCl thin film.
Photon energy of some peak is in good agreement
Peak structures with small radiative width don’t appear
This CuCl thin film is not so high-quality
DFWM spectrum in high-quality CuCl thin film (50℃)
results
 | measured thickness | substrate temperature
‘11 02/21 | 235nm | 50℃
High substrate temperature is important.
Thickness
235nm
6K
235 nm

## Slide 22
The difference between the crystal oscillator and measured thickness is not same (150℃), but it is same (130℃).
Summary
Evaporation on the substrate of CuCl thin film
Surface morphologies (150 and 130℃) are extremely-good.
Surface morphology
Sharp peak structures appear (150℃).
DFWM spectrum depends on the thickness of CuCl thin film.
DFWM spectrum
 | thickness | substrate temperature
Best condition | 329nm | 130℃

## Slide 24
Film thickness dependence
of calculated radiative decay time
Film thickness dependence
of calculated radiative width
Radiative width and decay time (310 and 329nm)
Previous results
n=5 exciton maintains high efficient radiative decay beyond nonradiative decay.
Optimizing the thickness of CuCl thin film will realize ultrafast radiative response than 10 fs.

## Slide 25: Reflection High Energy Electron Diffraction (RHEED)
substrate
e-beam
e-beam-exposed
CaF2 cap layer
40 nm
CaF2(111) substrate
CaF2 buffer layer
CuCl layer
40 nm
1 mm

## Slide 26
E-beam exposed
F defection
As
GaAs
Ga
H. C. Lee et al. Japan J. Appl. Phys. 26. 11. pp. L1834-L1836. 1987
CaF2
F
Growth of high-quality CuCl thin films
by e-beam exposed
Background

## Slide 27
過渡回折格子
プローブ光
ポンプ光
DFWM信号
２本のポンプ光が入射して、過渡回折格子が生成される。
過渡回折格子によって、プローブ光が回折される。
信号光が観測される。
縮退四光波混合(DFWM)
２本ポンプ光とプローブ光の時間差が０
非線形光学強度
ポンプ光間の時間差が０
過渡回折格子の緩和
Background
Notes: ２本のパルス光を同一箇所に照射すると、干渉によって励起子の励起を起こす。 これが回折格子としての役割を果たすため（過渡回折格子）、入射光の回折による信号光を観測できるようになります。

## Slide 28: CuCl CaF2
Zinc Blend
Cu+
Cl-
Fluorite
Ca2+
F-

## Slide 29
Future prospect
Fabricating the CuCl thin film (320~340nm, 130℃)
To keep high-quality of sample, fabricating cap layer
Measuring the quality of CuCl thin film by DFWM spectroscopy
CaF2 cap layer
40 nm
CaF2(111) substrate
CaF2 buffer layer
CuCl layer
40 nm
1 mm
329 nm
First
After
DFWM spectrum in a CuCl thin film having cap layer (<10K)
Leaving it out in the air for 30 hours
Saving CuCl thin film from degradation
Repeating experiments
Advantage of cap layer

## Slide 30
Transmission
results
’10 12/15
’10 11/18
 | crystal oscillator |  | measured thickness | 
’10 11/18 | 250nm |  | ×6.0 | 1500nm
‘10 12/15 | 165nm |  | ×6.0 | 988nm

## Slide 31
AFM image
results
 | crystal oscillator |  |  | measured thickness | growth rate
’10 11/18 | 250nm |  | ×6.0 | 1500nm | 0.32nm/s
‘10 12/15 | 165nm |  | ×6.0 | 988nm | 0.11nm/s
‘10 11/11 | 200nm |  | ×6.0? | 1200nm? | ?
‘10 11/18
40 nm
3 μm
‘10 12/15
3 μm
20 nm
‘10 11/11
3 μm
20 nm

## Slide 32
10,12/02
10,11/30
Transmission
results
 | crystal oscillator |  | measured thickness | 
’10 11/30 | 25nm |  | ×6.0 | 64nm
‘10 12/02 | 60nm |  | ×6.0 | 130nm

## Slide 33
AFM image
results
‘10 12/02
‘10 12/02
 | crystal oscillator |  | measured thickness |  | growth rate
‘10 12/02 | 60nm |  | ×6.0 | 130nm | 0.06nm/s
20 nm
3 μm