## Slide 1
Tanaka Lab. Yasushi Fujiwara
Three-dimensional-nanopatterned MgO substrates for the fabrication of epitaxial transition metal oxide nanowires
Notes: Hello, every one.
I am Yasushi Fujiwara from Tanaka laboratory.
This presentation title is three-dimensional-nanopatterned MgO substrates for the fabrication of epitaxial metal oxide nanowires.

## Slide 2: Contents
Introduction of keywords
  Strongly correlated electron system
  Merit of Nanostructures
  Nano processing procedure for metal oxides
My research
  Results of first semester
  Sidesurface of 3D-MgO
  Wulff’s theorem
  Approach to fabricate MgO(100) side surface
  Fabrication of MgO nanostructure
Conclusion
（強相関電子系酸化物）
（ウルフの定理）
Notes: At first, I introduce some keywords.
Strongly correlated electron system
Merit of Nanostructures, and nano processing procedure for metal oxides
Second, I will talk my research.
Results of first semester
Sidesurface of 3D-MgO
Wulff’s theorem
Approach to fabricate MgO(100) side surface, and Fabrication of MgO nanostructure
At Last, I will conclude my talk.

## Slide 3: Strongly correlated electron system
Science 285 1540 (1999)
Ferromagnetic(metal)
Paramagneic(insulator)
(La,Ca)MnO3
VO2
Insulator
metal
Science 318 14 (2007)
Strongly correlated electron system oxide have multi domains.
The phase separation occur due to strong electronic interaction.
100nm
400nm
（強い電子間相互作用）
Notes: First keyword is strongly correlated electron system.
Strongly correlated electron systems, such as transition metal oxide, show remarkable electronic phase separation and consist of mixed-phases.
The phase separate occur due to strong electronic interaction.
Left figure is VO2. This green region is metal phase, and blue region is insular phase.
Right figure is La, Ca, Mn, oxide.
This system has phase separation between red region ferromagnetic metal and yellow region insulator.
Strongly correlated electron system have mixed-phases whose domain size is a few tens to a few hundred nm.
Strongly correlate electron system have multi domain structure each phase.
These domains can be controlled, that is insulator domain change to metallic domain by applying external field.

## Slide 4: Merit of nanostructures
The nonlinear response by controlling single domain.
APL. 89 253121 (2006)
(La, Pr, Ca)MnO3
electrode
electrode
10μm~500nm
Nonlinear
response
（磁気抵抗）
Notes: Second keyword is nanostructures.
As I showed previous slide, the average domain size is about a few hundred nm.
This implies that the each phase can be trapped in the nanostructures, and this nanostructure expected to exhibit(イグジビット) giant response.
Indeed, it was reported nonlinear response in (La, Pr, Ca) MnO3 nanostructure.
This is a micro-nano channel structure of (La, Pr, Ca)MnO3, and magnetic resistance (MR) was measured with varying the width from ten μm to five hundred nm.
Here, the domain inversion from insulator to ferromagnetic metal was induced by applying magnetic field.
We can see insulator-metal transitions for all size channel structures.
We can see nonlinear response at 500 nm width, while 10 and 1 mm exhibit continuous change.
These figures are nano-channel systems increasing magnetic fields.
The insulator phases inversed to metal-conductive phases by magnetic field.
The sharp transition in the nano-channel structure can be illustrated(イラストレイト) in these schematic(スキマチック) images.
The nanostructure limits the percolative conducting pass of the ferromagnetic metal pass.
This nonlinear response in nanostructure indicates that the nanostructures which confined single domain expected to exhibit(イグジビット) the much giant response.
To achieve such response, the nanostructure whose size is less than the size of single domain is required.

## Slide 5: Purpose
High quality nanowire is required to produce the expected advantage.
External field
electrode
Electronic phase transition memory device
Ultrafast speed (80fs)
Lower switching energy
Giant nonliear response (>106)
Wire width
10 ~ 100 nm
< single domain size
（電子相転移メモリ）
（巨大非線形応答）
Notes: My purpose is to trap and control the strong correlated single domain by the external field and produce giant nonlinearly response.
Then wire width is less than single domain size, about ten nm – one hundred nm.
In the future, this nanostructure will be applied for electronic phase transition memory device, for example.
This device has advantages of ultrafast speed, lower switching energy, and giant nonlinear response.
So high quality nanowire is required to produce the expected advantage.

## Slide 6: Nano processing procedure for metal oxides
Pulse laser deposition
Bottom up
technique
Top down
technique
size
1nm
10nm
100nm
1000nm
productivity
Low
High
Mid
AFM lithography
Electron beam lithography
Nanoimprint
lithography
Photo lithography
Appl. Surf. Sci. 253 1758(2006)
Nano Lett. 9 1962(2009)
JJAP. 42 6721(2003)
2 µm
Nanotechnology 20 395301 (2009)
Notes: But metal oxides have high physical hardness and chemical stability.
So it is difficult to fabricate a few tens nanometer patterns with controlling shape and position.
This chart shows correlation chart of size and productivity.
Generally, to obtain nanostructures, top down techniques, for example photo lithography, EB lithography, nanoimprint lithography, and AFM lithography,
and bottom-up techniques, pulse laser deposition and so on, are applied.
Top down technique can control the position, and shape precisely(プレサイスリィ).
But it is difficult to fabricate a few nm size.
Bottom up technique can control size at atomic layer level.
But it is difficult to control position and shape of nanostructures.
I have been tried to fabricate the nanostructure by combining top down technique with bottom-up techniques,
so that the position, shape, and size controlled nanostructures can be fabricated.

## Slide 7: Fabrication of well-defined epitaxial nanostructure
substrate
Resist
substrate
Three dimensionally
nanopatterned MgO
(3D-MgO)
substrate
Oxide
Top down technique
Position and shape
Bottom up technique
Size at atomic layer level
The position, shape, and size controlled nanostructures can be fabricated.
Notes: I will show you three steps for fabrication of well-defined epitaxial nanostructure.
First step is resist nanopatterns by top down nanoimprint lithography.
The resist nanopatterns are high processing accuracy(アキュレイシィ) of side surface and high productivity and High reproducibility(プロデューシビリティ).
Second step is fabrication of MgO replica nanopatterns by bottom up pulse laser deposition and controlling MgO anisotropic growth.
MgO single crystal is used as a typical substrate for various epitaxial oxides.
MgO nanopatterns are enable high temperature deposition, which produce epitaxial oxide nanostructures.
Third step is high quality oxide nanostructures by glancing angle deposition of PLD.
As we deposit target oxide materials on the 3D-patterned MgO substrate by controlling the deposition thickness,
we can obtain the expected size nanostructures while retaining the original position and shape.
In Today’s presentation, I show fabrication of MgO nanopattern substrate.

## Slide 8: Detail fabrication procedures
MgO substrate
MgO substrate
MgO substrate
MgO substrate
MgO substrate
1.cleaning substrate
4.RIE(CF4,O2)
5.PLD(MgO)@RT
6.removing resist
7.annealing
resist
MgO substrate
8.PLD&ECR
MgO
oxide
MgO substrate
2.spin coating
MgO substrate
3.nanoimprint
mold
Three dimension MgO nanowire
nanowire
（反応性イオンエッチング）
Notes: This slide show detail fabrication precedures.
First, cleaning substrate.
Second, resist is spin coating.
Third, nanoimprinting to obtain original patterns.
Fourth, removing extra resist by Reactive Ion Etching.
Fifth, MgO deposited by PLD. Here, I should keep the substrate temperature at RT since the resist patterns are broken about two hundred degree Celsius.
Sixth, removing resist.
Seventh, annealing in order to crystalize MgO.
At Last, 3D-MgO substrate is used for the 3D oxide nanostructure.

## Slide 9
STO(002)
STO(003)
MgO(022)
STO substrate
STO substrate
3D-MgO
MgO crystallization condition by postanneal
MgO was crystallized by postannealing at 1000℃.
Notes: I will show results.
I studied MgO crystallization temperature on STO(001) substrate using XRD.
Because of room-temperature deposition, as-grown MgO was not crystallized.
This figure show XRD curves for MgO deposited on STO(001) substrate with changing annealing temperature.
Three peaks appeared.
Two peak is STO substrate peak.
This peak is MgO(022) peak.
At seven hundreds degree celsius(セルシウス), this peak is appeared but small.
At one thousand degree celsius, this peak become intense.
This result show that MgO was crystallized by posetannealing above 700 degree Celsius and crystal quality improved with increasing temperature.
I decided the postannealing temperature is 1000 degree Celsius in this study.
9

## Slide 10: Anisotropic growth of MgO
Schematic diagram
[100]
[010]
substrate
500nm
Zig-Zag line
MgOsubstrate
[100]
[010]
500nm
Parallel line
MgOsubstrate
3D-MgO
[001]
MgOsubstrate
3D-MgO
[100]
[010]
MgOsubstrate
[110]
[110]
[001]
[001]
500nm
3D-MgO
MgOsubstrate
After anneal
(1000℃)
Before anneal
MgOsubstrate
3D-MgO
500nm
[001]
[100]
[010]
[110]
[110]
[001]
[001]
[110]
[110]
3D-MgO
3D-MgO
（異方性成長）
Notes: It is known that MgO show strong anisotropic growth.
Therefore, I fabricate MgO nanopatterns of different direction against substrate to confirm anisotropic growth of MgO.
Left SEM image is before annealing nanopatterns.
Right SEM image is after annealing nanopattarns.
Although, there are little differences of the sidesueface structures among [010]-parallel and [110]-parallel MgO wires before annealing, quite different sidesurface structures were obtained after annealing.
[100] parallel wire had zigzag edge structures, and [110]-parallel wire had straight flat edge structure.
This difference is caused by MgO anisotropic growth and I will discuss them later.
10

## Slide 11: Structure analysis of MgO nanowire (TEM)
200nm
MgOsubstrate
3D-MgO
MgOsubstrate
3D-MgO
10nm
I confirmed that quality of crystallized 3D-MgO is similar to that of MgO substrates.
Crystal relation: 3D-MgO(001)[100]//MgOsubstrate(001)[100].
3D-MgO (FFT)
MgO substrate(FFT)
Fracture
direction
[110]
（結晶方位関係）
（FFT : 高速フーリエ変換）
（透過型電子顕微鏡）
Notes: I analyzed crystal structure of 3D-patternd MgO substrate by cross-section TEM.
Left figure is TEM image across the wire line
Right figure is magnified(マグニファイト) image of nanopattern edge.
These figures are FFT images 3D-MgO and MgO substrate regions.
The points in MgO substrate are coincident with those in 3D-MgO region.
So I confirmed that crystal quality of 3D-MgO is similar to that of MgO substrates.
TEM image also showed Crystal relation is 3D-MgO(001)face[100]derection//MgOsubstrate(001)face[100]direction.
11

## Slide 12: Sidesurfaces of 3D-MgO
The angle between sidesurface and substrate surface is 55º.
Therefore, sidesurface is MgO(111).
100nm
MgO substrate
3D-MgO
Crosssection SEM image
: Mg
: O
[100]
[010]
substrate
500nm
Zig-Zag line
3D-MgO(001)
MgO(001)substrate
500nm
Parallel line
MgO(001)substrate
3D-MgO(001)
[001]
[001]
After anneal (1000℃)
[110]
[100]
[100]
[010]
[110]
[110]
(111)
(111)
MgO(100)
MgO(110)
MgO(111)
To fabricate oxide nanowires, the straight sidesurfade is better,
that is, I want 3D-MgO nanowire with (100) sidesurface.
Notes: This figure is cross-section SEM image of [110]-parallel wire.
They are schematic MgO (100), (110), and (111) crystal face.
The angle between sidesurface and substrate surface is fifty five degree.
This implies sidesurface is MgO(111) face. The (111) sidesurface consistent with the zig-zag edge on [010]-parallel line.
Therefore, I conclude sidesurface is (111)face.
To fabricate oxide nanowires, the straight sidesurface is better, that is, I want 3D-MgO nanowires with (100) sidesurface.
12

## Slide 13: Wulff’s theorem
Deposited MgO
MgO substrate
Crystallized MgO
J. Chem. Soc., Faraday Trans. 92 433(1996)
Crystal face | Surface energy
(100) | 1.25 J/m2
(110) | 3.02 J/m2
(111) | 3.86 J/m2
In fact
Crystallized MgO
Wulff’s relational expression
Surface energy
distance to surface
MgO substrate
MgO substrate
expectation
According to crystal surface energy we expected to produce (100) face.
Bulk MgO (calc.)
（表面エネルギー）
Notes: I thought the key point in obtaining (100) sidesurface is to control surface energy of MgO face.
The surface stability(スタビリティ) is expressed by Wulff’s theorem. According to Wulff’s relation, surface energy over distance to surface is constant.
σ is surface energy. h is distance to surface.
Equilibrium(イクィリブリアム) crystal shape is decided by surface energy.
This figure is how to illustrate equilibrium crystal shape by wulff’s relational expression.
For MgO crystal faces, surface energy of each surface is reported as shown in this table.
We can see (100) phase is most stable(ステイブル).
According to crystal surface energy we expected to produce (100) surface.
Indeed, sidesurface of crystallized MgO was (111). It was reported (111) surface energy reduces by surface contamination and so on.
In this case, the surface energy of (111) may be close to that of (100) value.
13

## Slide 14
Equilibrium crystal shape
on substrate
γ = 0
γ = σA
0 < γ < σA
σA < γ < 2σA
MgO substrate
(111)
MgO substrate
(100)
Case of low-aspect ratio
σ(100) < γ < 2σ(100)
Case of high-aspect ratio
0 < γ < σ(100)
expectation
Approach to fabricate MgO(100) side surface
Sidesurface could be changed from (111) face to
(100) face by increasing the aspect ratio.
「結晶成長（材料学シリーズ）」（丸善） 後藤芳彦
（接着エネルギー）
Notes: In addition to surface energy(エナジー), Equilibrium crystal shape on substrate is decided by value of adhesive energy between crystal and substrate.
γ is adhesive energy.
This figure shows the relationship between crystal and substrate defined with γ and σ.
Case of γ equal 0, a crystal does not contact on substrate.
Case of γ equal σ, half of crystal is buried(ベリード) in substrate.
Case of γ is less than σ and bigger than 0, a part of crystal is located on substrate.
Case of γ is less than 2σ and bigger than σ, almost all parts of crystal is located on substrate.
This relation provide us one scenario:
Sidesurface could be changed from (111) facet to (100) face by increasing the aspect ratio.
14

## Slide 15
MgO substrate
MgO
MgO substrate
Removing resist
Sidewall deposition@RT
MgO substrate
Annealing 1000℃
Fabrication of MgO nanostructure
Modify Fabrication process
300nm
MgO substrate
6.removing resist
MgO substrate
7.annealing
MgO substrate
5.PLD(MgO)
MgO
500nm
annealing
Temperature:1000℃
O2 pressure:10-4Pa
[001]
[010]
[100]
[001]
[010]
[100]
Notes: To increase the aspect ratio, I modified fabrication process.
Upper is previous process.
Bottom one is modified process.
I modified deposition method from normal deposition to sidewall deposition.
Sidewall deposition produced high aspect ratio MgO nanowires as shown in this figure.
Right figure is after annealing at one thausand degree. We can see the nanowires with flat (100) sidesurface.
I succeed to fabricate the three dimensional nanopatterned MgO substrates.
15

## Slide 16: Conclusion
I tried to fabricate the three dimensionally nanopatterned MgO substrates.
I found that sidesurface of MgO nanowire was (111) face at low aspect ratio.
I modified the fabrication process, and succeed in fabrication of the MgO nanowires structure with flat (100) sidesurface.
I have been trying to fabricate nanowire structures on the 3D-MgO nanowire substrate, and study their magnetic properties.
Future plan
MgO substrate
MgO substrate
Notes: At last, I Conclude my talk.
I tried to fabricate the three dimensionally nanopatterned MgO substrates.
I found that sidesurface of MgO nanowire was (111) face at low aspect ratio.
I modified the fabrication process, and succeed in fabrication of the MgO nanowires structure with flat (100) sidesurface.
In the Future plan.
I have been trying to fabricate nanowire structures on the 3D-MgO nanowire substrate, and study their magnetic properties.
Thank you for your kind attention.
16