## Slide 1: Terahertz spectroscopy of electromagnons in Multiferroics
Ashida lab.
Saito Tadtaka

## Slide 2: Contents
Introduction
---Multiferroic materials
---The mechanism of Electromagnon’s excitation
Experiment
---Experimental set up
---Sample
Results
Summary

## Slide 3
Multiferroics
E
H
P
M
Multiferroics are materials where ferroelectricity and
ferromagnetism are inherently coupled.
The magnetization can be controlled by electric field of light.
The polarization can be controlled by magnetic.
Introduction ---Multiferroic materials
Magnet Electric effect
(ME effect)

## Slide 4: Magnet Electric effect
Antisymmetry Dzyaloshinskii-Moriya interaction
Ptotal //c
Spiral-spin-order
a
b
c
らせんスピン磁性
bc-spiral
Introduction ---Multiferroic materials

## Slide 5: Electromagnon
Magnon can be excited
by electric field of light.
Magnon
Spin wave
Magnon is exited by magnetic field.
Multiferroics…
Electromagnon(2006)
RMnO3 R; rare-earth metal
Low temperature, High H
Introduction ---electromagnon’s excitation
N.Kida. et al Opt. Soc 26 108794(2009)

## Slide 6
RMnO3
Rare-earth-metal perovskite magnites
R; rare earth elements(Y, Eu, Tb, Dy, ・・・)
M. Mochizuki, et al Phy. Rev. Lett.104.177206(2010).
Introduction ---electromagnon’s excitation

## Slide 7
Phase Diagram of Eu1-xYxMnO3
Spiral spin phase
Spontaneous polarization
Spin chirality
At ab-cycloidal…
Introduction ---electromagnon’s excitation

## Slide 8
Super Exchange Interaction
Introduction
The modulation of this interaction results in
electromagnon’s excitation.
Introduction ---electromagnon’s excitation

## Slide 9: Mechanism of Electromagnon
E//a
E//b
a
b
Introduction ---electromagnon’s excitation

## Slide 10: Experimental set up
Experiment
THz-TDS enables us to observe
a waveform of ”E(t)” directly.
By using THz-TDS ,
both amplitude and phase of ”E(t)” are directly obtained.

## Slide 11
Y-type hexaferrite Ba2Mg2Fe12O22
Ferri magnetic
proper screw
Conical spin
Room temperature
T<195K
T<50K
Sample
六方晶フェライト
S. Ishiwata et al Science 319, 1643 (2008)

## Slide 12
Weak magnetic field(～1T)
H//[001]
Longitudinal conical spin
H(>3T)
H//[100]
Transverse conical spin
H(＞4T)
Ferrimagnetic
Proper screw
Ferrimagnetic
θ
(001)
(100)
(120)
Transition of spin phase by weak magnetic field
Sample

## Slide 13: Spectra change
Proper-screw
Conical
Ferri
F
C
F
C
F
Proper-screw
Conical
Ferri
F
C
C
F
F
Sample
Electromagnon’s excitation
was observed in
conical spin order.
Spectra change by weak H
E//(001)
N. Kida et al Phy Rev B 83, 064422 (2011)

## Slide 14: Z-type hexaferrites Sr3Co2Fe24O41
Y-type
Z-type
Sample
Y. Kitagawa, etc Nat. Mat. 9, 797(2010).
Polarization by ME effect
at room temperature.
c

## Slide 15: Results
Results

## Slide 16: Results
Results

## Slide 17: Summary
I introduced to my study toward observation of electromagnon’s excitation at room temperature.
We observed the change of spectrum by the direction of light polarization in Z-type hexaferrites Ba3Co2Fe24O41 at room temperature.
Summary