## Slide 1: Optical fabrication and Optical manipulation of semiconductor nanoparticles
Ashida lab. Nawaki Yohei

## Slide 2: Contents
Introduction
  Optical fabrication and manipulation
  Advantage of particles
  Photo Induced force
  Resonant force
Purpose
  Previous study
  My study
Experimental setup
  Ablation and Manipulation
  Scanning electric microscopy
Optical fabrication
  Tablet of GaN
  Crystal of GaN
Optical manipulation
  Zinc oxide
Summary

## Slide 3: Ablation and manipulation
Introduction
Ablation laser
Manipulation laser
Ablation
Fabrication method of particles
using laser sputtering
Manipulation
Transporting method by the resonant radiation force
Si substrate

## Slide 4: Low-dimensional structures
Introduction
DOS
DOS
DOS
DOS
E
E
E
E
Bulk
Thin film
Quantum wire
Nano particle
enhancement of oscillator strength

## Slide 5: Photo induced force
Introduction
Gradient Force
Scattering and Absorption pressure
Optical axis
Photo induced force
Gradient force
Scattering and Absorption pressure
Photo induced force: 光誘起力
Gradient force: 勾配力
Scat. And abs. pressure: 散逸力

## Slide 6: Gradient force
Introduction
The force pushing objects to the focal point
Stabilization point
Electrical gradient
Gaussian beam

## Slide 7: Scattering and Absorption force
Introduction
The force arising from the momentum transfer from the light
power
scattering
absorption

## Slide 8: Manipulation in various scale
Introduction
Microparticle
Nanoparticle
Atom
1mm~
1nm~1mm
~1nm
Optical tweezers
Structural dependence
No Structural dependence
Laser cooling
No resonance
resonance
Structural dependence
resonance
or
No resonance
It’s difficult
for optical manipulation.

## Slide 9: Resonant or Non-resonant light
Energy of applied light
≠
Energy of exciton level
Energy of applied light
=
Energy of exciton level
Introduction
Non resonant
Resonant
Resonant
Resonant
E
a

## Slide 10: Enhancement by resonant light
Introduction
Ref: T.Iida and H. Ishihara Phys. Rev. Lett. 90, 057403 (2003)
Using resonant light
Photo induced force is drastically enhanced.
Numerical calculation example (CuCl)
100 times of gravitational acceleration

## Slide 11: Previous study
Purpose
Our group has succeeded manipulation of nanoparticles
Wide-gap semiconductor
CuCl
ZnO
K. Inaba phys.stat.sol. (b)243, No.14, (2006)
S. Okamoto master thesis (2011)

## Slide 12: My study
Purpose
GaN bulk
GaN particles
Manipulated GaN particles
ablation
manipulation

## Slide 13: Fabrication method
Experimental setup
Nd:YAG
Ti:sapphire
ablation laser
manipulation laser
wavelength :525nm
pulse duration :10ns
SHG
wavelength :726nm
cryostat
Si substrate
sample
back substrate
front substrate
Vacuum state (300K)
Superfluid He state (2K)
wavelength :718nm
pulse duration :100fs

## Slide 14: Observation method
Experimental setup
Electron beam
Secondary electron
sample
Character X-ray
Cathode Luminescence
SEM measurement
CL measurement
Energy Dispersive X-ray Spectrometry
Scanning electron microscope
Scanning electron microscope: 走査型電子顕微鏡
Secondary electron: 二次電子
Cathode luminescence :電子線励起による発光
Character X-ray: 特性X線
To analyze element
To take 2D image

## Slide 15: Optical fabrication

## Slide 16: Gallium Nitride
Ablation
GaN: 3.4eV
cf. ZnSe, SiC, ZnO, CuCl
GaN has wide controllable range of bandgap
with ternary crystal semiconductor InN, AlN.
0.7eV~6.1eV
Crystal growth is difficult
Blue- and UV-Light emitting diode and laser
Wide-gap semiconductor

## Slide 17: Tablet of GaN
Ablation
Press!
Powder
Tablet

## Slide 18: SEM images
Ablation
Ablation conditions
Vacuum state
Nd:YAG power 0.5mJ
I could fabricate particles...

## Slide 19: Element analysis
Ablation
EDS data
Ga mapping image
SEM image
Nitrogen peak was expected.

## Slide 20
Particles were oxidized.

## Slide 21: Crystal of GaN
Ablation
Crystal
Tablets included many impurity.
The reason why is that oxidized particle were fabricated.
The surface of powders were oxidized.
I used crystal of GaN

## Slide 22: SEM image
Ablation
Vacuum state
Ablation conditions
Nd:YAG power :1.5mJ

## Slide 23: Element analysis
Ablation
A broken piece by ablation
Ga mapping image
SEM image
EDS data
Nitrogen was observed.

## Slide 24: Element analysis
Ablation
Fabricated particle by ablation
Ga mapping image
SEM image
EDS data
Nitrogen peak was expected.

## Slide 25
Particles have nitrogen defect.

## Slide 26: Superfluid Helium condition
Ablation
Superfluid Helium
Low temperature
Viscosity becomes zero.
Resonant energy very sharp
Small destabilizing effect
Suitable for optical manipulation
The particles can be cool rapidly.
For ablation

## Slide 27: Crystal of GaN
Ablation
Superfluid He state
Ablation conditions
Nd:YAG power 0.5mJ

## Slide 28: Crystal of GaN
Ablation
Ga mapping image
SEM image
Nitrogen peak was expected.
EDS data

## Slide 29
Particles have nitrogen defect.

## Slide 30: Results
Ablation
The particles had nitrogen defect and contained oxygen.
Tablet from powder
Vacuum condition
superfluid He condition
In such condition
Crystal
Vacuum condition
superfluid He condition

## Slide 31: Optical manipulation

## Slide 32: Zinc Oxides
manipulation
Band-gap energy of ZnO is 3.4eV.
Wide-gap semiconductor
1mm
1 cm
Polygonal shape
ZnO is very stable material, because It’s oxidation products.

## Slide 33: Problem of size distribution
manipulation
Advantage of particle
Density of state
Size distribution
Density of state becomes cloudy.
Density state become sharply.

## Slide 34: Pulse laser spectra
manipulation
Pulse duration
Peak energy
Spectrum width
1ps
100fs
3.38eV
3.38eV
2meV
20meV
fs pulse laser
ps pulse laser
Resonance radius
under 100nm radius
specific radius
Y. Saito Master thesis (2009)

## Slide 35: Decrease of size distribution
manipulation
Y. Saito Master thesis (2009)
fs pulse laser
ps pulse laser
The Size distribution reduced in response to spectrum width.
I try to measure size distribution from spectrum width of photoluminescence.

## Slide 36: Summary
Optical fabrication
I can’t fabricate GaN particles
Optical manipulation
The particles fabricated by ablation
have nitrogen defect and contained oxygen.
I try to measure size distribution from spectrum width
of photoluminescence.

## Slide 37: Appendix

## Slide 38: Photo induced force
Appendix
Gradient force
Radiation pressure
Optical letters vol.11, No. 5, 288 (1986)

## Slide 39: First experiment
Appendix
transparent latex spheres
size
material
0.59, 1.31, 2.68mm
CW argon laser
l = 0.5145mm
w0= 6.2mm
Power 19mW
The author measured sphere moved at 26±5mm/sec
samples
laser
TEM00

## Slide 40: Laser cooling

## Slide 41: Quantum confinement
Appendix
a > ab
a :ドット半径
ab :励起子ボーア半径
ドット内に励起子が閉じ込められる
2a
2ab
ΔE
量子サイズ効果によりエネルギーレベルが変化
2a
弱閉じ込めモデル
2a
2ab
ab > a
強閉じ込めモデル
励起子ボーア半径
CuCl
ドット半径
0.68nm
数nm
弱閉じ込めモデル
励起子の重心運動が量子化