## Slide 1: Distinct Fermi Surface Topology and Nodeless Superconducting Gap in a (Tl0.58Rb0.42)Fe1.72Se2 Superconductor
D. Mou et al
PRL 106, 107001 (2011)
Kitaoka Lab.
Keisuke Yamamoto

## Slide 2: Contents
Introduction
  Iron based superconductor
    Electronic structure
  AxFe2-ySe2 (A = K,Tl,Cs,Rb,etc.)
    Characteristic
Experiment and result (Tl0.58Rb0.42)Fe1.72Se2
  ARPES(角度分解光電子分光）
  Fermi surface
Summary
Future work

## Slide 3: Iron-based superconductor
LaFeAsO
BaFe2As2
LiFeAs
FeSe
Fe
As
Se
1111 system
122 system
111 system
11 system
Tc max = 55K
Tc max = 38K
Tc max = 18K
Tc max = 8K
Fe-Pnictide layer
Introduction
Pnictgen(15族元素)

## Slide 4: Iron-based superconductor
Introduction
Band structure
Fermi suface
Phase diagram
hole
electron
nesting
hole
electron
electron scattering

## Slide 5: Electron-dope
hole
Introduction
Band structure
εF
k
electron
Electron-dope
nesting
Electron-dope
Fermi suface
E

## Slide 6: AxFe2-ySe2
Fe vacancy
Phase diagram
Band structure
hole
Fermi surface
Qian et al , arXiv:1012.6017v1 Dec (2010)
M.H.Fang et al , EPL, 94 (2011) 27009
M.H.Fang et al , EPL, 94 (2011) 27009
Motivation
electron
Fe-atom
vacancy
Absence of the hole band
Notes: Blue solid circle: Fe-atom; green hollow circle: vacancy

## Slide 7: AxFe2-ySe2
Many differences from previous Iron-superconductor
  Existence of Fe vacancies
  Impossible for the electron scattering
Why the Tc is high (over 30K) ?
Observe the electron structure of this sample by ARPES
Motivation

## Slide 8: (Tl0.58Rb0.42)Fe1.72Se2
Experiment
Tl,Rb
Fe
Se
M.H.Fang et al , EPL, 94 (2011) 27009
H.D.Wang et al , EPL, 93 (2011) 47004
Parameter

## Slide 9: ARPES(angle-resolved Photoemission Spectroscopy)
one of the most direct and powerful methods of studying the electronic structure dispersive with the crystal momentum in strongly anisotropic systems
crystal surface
exiting light
Pin// = Pout//
measure both momentum and kinetic energy of the electrons photo emitted from a sample
Experiment

## Slide 10: Fermi surface
Result
D. Mou et al PRL 106, 107001 (2011)
Two electronlike Fermi suface sheets, α and β around Γ
D. Mou et al PRL 106, 107001 (2011)

## Slide 11: Fermi surface
hole
g
electron
Result
hole
g
Early report on KFeSe
electron
In this paper (Tl,Rb)FeSe
Question : What is origin of the electronlike β band around Γ ?
3 possibilities
Whether it could be a surface state
Whether the β band can be caused by the folding of the electronlike γ surface near M
Whether the measured β sheet is a Fermi surface at a special kz cut

## Slide 12: Fermi surface
Result
D. Mou et al PRL 106, 107001 (2011)
Superconducting gap
Dash line is a BCS gap form
Gap size
The temperature dependence of the gap size roughly follows the BCS-type form
Notes: To visually inspect the Possible gap opening and remove the effect of the Fermi distribution function near the Fermi level, we have symmetrized these original EDCs

## Slide 13: Fermi surface
Result
D. Mou et al PRL 106, 107001 (2011)
β Fermi surface displays a clear superconducting gap
The peculiar tiny α pocket near Γ, we do not find signature of clear superconducting gap opening

## Slide 14: Super conducting gap
D. Mou et al PRL 106, 107001 (2011)
T =15K
Result
Fermi surface |  |  | 
Gap size | 12±2 meV | 15±2 meV | 
 | 9 | 11 | 
Fermi surface |  |  | 
Gap size | 12±2 meV | 15±2 meV | 
 | 9 | 11 | 
Nearly isotropic gap
Without gap nodes
3.52 (BCS)

## Slide 15: Summary
We have identified a distinct Fermi surface topology in the new (Tl0.58Rb0.42)Fe1.72Se2 superconductor
Near the Γ point, two electronlike Fermi surface sheets are observed
hole
g
electron
electron scattering
Interband scattering between the electronlike Fermi surface sheet near Γ and electronlike Fermi surface sheet near M gives rise to electron pairing and superconductivity
Interband scattering : バンド間散乱