## Slide 1: Photo-excited carrier dynamics revealed with terahertz pump-probe spectroscopy for opposite travelling direction of excitation pulse and terahertz pulse
Ashida Lab・M1
Masahiro Yoshii

## Slide 2: Contents
Introduction
  terahertz wave
  characters of Si
  observation of carrier dynamics
  opposite arrangement
Previous Work & Purpose
Experimental Setup
  THz time domain spectroscopy (THz-TDS)
  THz pump optical probe spectroscopy
Result & Discussion
Summary & Future Plan

## Slide 3: terahertz wave
Introduction
Wavelength
Frequency(Hz)
300km
300m
300mm
300μm
300nm
300pm
300fm
103
106
109
1012
1015
1018
1021
microwave
THz region
visible
X-ray
Wavelength
Frequency(Hz)
3cm
3mm
300μm
30μm
3μm
300nm
0.01THz
0.1THz
1THz
10THz
100THz
1000THz
THz region
FIR
MIR
NIR
1THz = 300μm =4.1 meV=48K
gap of low-Tc superconductor
mode of collective oscillation of macromolecule

## Slide 4: characters of Si
Introduction
        indirect band gap semiconductor
        diamond structure
5.43Å
        band gap energy : Eg : 1.12eV
                Г25’-X1 : 1.2eV
        Г25’-L1 : 2.0eV
        Г25’-Г15 : 3.4eV
        Г25’-Г2’ : 4.2eV
        α0 at 800nm : 942cm-1
        ↕
        penetration depth : 10.6μm
光物性ハンドブック , P42
Eg

## Slide 5: observation of carrier dynamics
Introduction
thickness of sample < penetration depth
⇒transmission arrangement
thickness of sample > penetration depth
⇒reflection arrangement
excitation light
excitation light

## Slide 6: opposite arrangement
Introduction
R
reflection arrangement
opposite arrangement
excitation light
ω
carrier density
excitation light
ω
reflectivity
  intrinsic characters of carriers
  spatial distribution of carriers
reflectivity
  intrinsic characters of carriers
  phase shift
  spatial distribution of carriers
ω/ωp
reflectivity of Drude model

## Slide 7: Previous Work & Purpose
GaAs ：PHYSICAL REVIW B 70, 125205 (2004)
Si：Tsubouchi, Yokoyama, Nagai, Oshima, 応用物理学会 2011秋 2a-F-2
Tsubouchi observed carrier dynamics of Si up to 2THz.
○phase shift
×reflectivity
⇓
I did this work over 2THz.
reflectivity
phase shift

## Slide 8: THz time domain spectroscopy
Experimental Setup
l/4
ND
REGEN
l/2
BBO
GaAs
WP
BD
sample
Si
EO sampling

## Slide 9: THz pump optical probe spectroscopy
Experimental Setup
l/4
ND
REGEN
TOPAS
ND
BPF
prism
l/2
BBO
GaAs
WP
BD
sample
Si
EO sampling
THz-TDS

## Slide 10: opposite arrangement
Experimental
Setup
(a)
対向配置
通常の 反射配置
ω
(b)
Pump光
(c)
t
THz光
Pump光
traditional reflection arrangement
complex reflectance
      spatial distribution
      intrinsic characters
opposite arrangement
complex reflectance
      intrinsic characters
phase shift
      spatial distribution

## Slide 11: measured waveforms
Result
temporal advance of the waveform
→ shift of the reflective interface
decrease of the electric field amplitude
→ absorption by the photo-excited
carriers

## Slide 12: reflectivity
Result
carrier density dependence of reflectivity
Plasma absorption shift to higher
frequency side.
The position of plasma absorption
gives close agreement with the
calculated data.
・・・: calculated data (τ=100fs)

## Slide 13: phase shift
carrier density dependence of phase shift
Phase shift increase.
The spectrums are not same with
the calculated date.
    data mismatching of spatial
distribution
・・・: calculated data (τ=100fs)
Result

## Slide 14: difference from calculated data
Result
When we calculated, we assumed that the relaxation time of carriers does not depend on the carrier density.
but
We find that the relaxation time of carriers changes when the carrier density is over 1017cm-3.
PHYSICAL REVIEW B 75, 233202 (2007)

## Slide 15: correction of calculated model
Result
τ : constant
PHYSICAL REVIEW B 75, 233202 (2007)

## Slide 16: reflectivity and phase shift
Result
reflectivity
phase shift

## Slide 17: Conclusion
I constructed a novel experimental setup of THz pump-probe
spectroscopy.
(the opposite arrangement of the excitation light and the probe light)
I observed the THz wave reflected at the rear surface of the sample.
I distinguished the information on spatial distribution and that on
intrinsic characters of photo-excited carriers. (>2THz)
I determined that the scattering time of carriers is about 100fs.
But, the SN of observed spectrums are too bad to discuss about the
results of reflectance and phase shift.

## Slide 18: Future Plan
I’ll understand why the relaxation time
changes by carrier density.
I try to change the wavelength excitation light.
(wavelength dependence)

## Slide 19
補助スライド

## Slide 20: 坪内さんによる先行研究
π shift
carrier density dependence of peak position

## Slide 21: 永井先生による理論結果

## Slide 22: 大気プラズマからのテラヘルツ発生
破壊閾値が存在しない
位相整合条件などによる帯域の制約がない
⇒高強度・広帯域のテラヘルツ発生
大気プラズマにωと2 ωの光を入射する
⇓
電荷分布に非対称性が生じる
⇓
双極子として振る舞い、テラヘルツ発生
Laser & Photon. Rev. 1, No. 4, 349–368 (2007) / DOI 10.1002/lpor.200710025

## Slide 23: EOサンプリング